Notes :

- The composition of the grades present in this PDF is accurate. The data sheets provided to you as a separate attachment - kindly edit the values of the composition there as per this sheet.

- This is the required content. Kindly present according to the website colour scheme. Wherever necessary, provide the details in tabular form such as chemical composition, size ranges etc (in whatever way it looks good).

1.  D2 Steel Grade:

Grade Brief:

Toolman Special Steels is proud to produce and offer D2 (1.2379) - a high-carbon, high-chromium tool steel known for its excellent wear resistance and stability. It is commonly used for tools requiring high resistance to abrasive and adhesive wear. It is characterised by high wear resistance, superior ductility, extremely low deformation, and hardening crack tendency. It has very high hardenability and significant dimensional stability during the quenching process.

Steel Properties

- Wear resistance

- Impact resistance

- Fine grain size

- Uniform distribution of carbide

- High toughness

- Extremely low gas content

- Good cleanliness

Specifications

Chemical Composition

| Element | Min (%) | Max (%) |
| --- | --- | --- |
| C | 1.4 | 1.6 |
| Si | 0.10 | 0.6 |
| Mn | 0.1 | 0.6 |
| P | - | 0.030 |
| S | - | 0.030 |
| Cr | 11 | 13 |
| Mo | 0.7 | 1.2 |
| V | 0.5 | 1.1 |

Mechanical Properties:

| Property | Value |
| --- | --- |
| Hardness (HBW) | 255 max (Annealed) |
| Quenching and Tempering Hardness (HRC) | 59 min (Annealed) |
| Poisson’s Ratio | 0.27-0.30 |
| Impact Toughness | 77 J/cm2 |
| Tensile Strength | 1860-2060 MPa |
| Yield Strength | 1600-1800 MPa |

Physical Properties

| Property | Value |
| --- | --- |
| Density (g/cm³) | 7.7 |

Modulus of Elasticity

| Temperature (°C) | GPa |
| --- | --- |
| 20 | 210 |

Thermal Properties

Thermal Expansion Coefficient

| Temperature (°C) | Thermal Expansion Coefficient (10^-6/°C) |
| --- | --- |
| 400 | 13.8 |
| 500 | 14.1 |

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 20 | 20 |

HEAT TREATMENT AND PROCESSES

| Process | Temperature (°C) | Duration | Cooling Method |
| --- | --- | --- | --- |
| Soft Annealing | 820 - 850 | 2-5 hours | furnace |
| Stress Relief Annealing | 600 - 650 | min 4 hrs | Furnace |
| Hardening | 1000 - 1050 | Group III | oil, air, WB 500°C |
| Tempering | 480 - 580 see tempering curve | min 2 hrs Depending on cross section | still air |

| Tempering °C after quenching | 100 | 200 | 300 | 400 | 500 | 525 | 550 | 600 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| HRC | 63 | 61 | 58 | 58 | 59 | 58 | 56 | 51 |

Applications

- Punches and dies

- Shear blades

- Tooling for plastics

- Tyre Shredders

- Cold forming tools

- Rollers and knives for industrial cutting applications

- High performance cutting tools, stamping, woodworking, drawing, deep drawing and pressing tools

- for ceramics and pharmaceutical industries, rolls, measuring tools, plastic moulds, shear blades

Quality Assurance

Our  D2 1.2379 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our D2 1.2379 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

SIZE RANGE

Products                             Diameter (mm)

Hot Rolled bar                       8 - 65

Forged and Turned bars        65.2 - 500

Forged Square Bars              50 - 500

FLATS

THICKNESS                     WIDTH

6.00 mm - 410.00 mm       20.00 mm  - 700.00 mm

Click here to contact our experienced sales team who will assist you with your D2 1.2379 tool steel enquiry.

2.  D3 Steel Grade:

Grade Brief:

Toolman Special Steels is proud to produce and offer D3 (1.2080) - a high carbon and high chromium tool steel. It has superior wear resistance and good dimensional stability with high compressive strength. It hardens with a very slight change in size. The alloy possesses very high compressive strength and is deep hardening.

Steel Properties

- ˙Wear resistance

- ˙Impact resistance

- ˙Fine grain size

- ˙Uniform distribution of carbide

- ˙High toughness

- ˙Extremely low gas content

- ˙Good cleanliness

Specifications

Chemical Composition

HCHCR-D3    DIN 2080   AISI D3     AFNOR Z210CW12-01

| C | Si | Mn | P | S | Cr | V |
| --- | --- | --- | --- | --- | --- | --- |
| 2.00 - 2.35 | 0.10 - 0.60 | 0.10 - 0.60 | 0.03 | 0.03 | 11.0 - 13.5 | 1.00 |

Mechanical Properties:

| Property | Value |
| --- | --- |
| Annealing Hardness (HBW) | 248 max |
| Quenching and Tempering Hardness (HRC) | 60 min |
| Poisson’s Ratio | 0.27-0.30 |
| Impact Toughness | 28 J/cm2 |

Physical Properties

| Property | Value |
| --- | --- |
| Density (g/cm³) | 7.7 |

Modulus of Elasticity

| Temperature (°C) | GPa |
| --- | --- |
| 20 | 190 |

Thermal Properties

Thermal Expansion Coefficient

| Temperature (°C) | Thermal Expansion Coefficient (10^-6/°C) |
| --- | --- |
| 20 -100 | 12 |

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 20 | 16.6 |

HEAT TREATMENT AND PROCESSES

| Soft annealing °C | Cooling | Hardness HB |
| --- | --- | --- |
| 810 - 850 | Furnace | max. 250 |

| Stress-relief annealing °C | Cooling |
| --- | --- |
| approx. 670-720 | Furnace |

| Hardening °C | Quenching | Hardness after quenching HRC |
| --- | --- | --- |
| 940 – 970 | Oil | 64.5 |
| 950-980 | Air (up to 30 mm thickness) | 64.5 |

| Tempering °C after Quenching | 100 | 200 | 300 | 400 | 500 | 600 |
| --- | --- | --- | --- | --- | --- | --- |
| HRC | 63.5 | 61.5 | 58 | 57.5 | 55 | 47 |

Applications

- Punch

- Cold-rolling intermediate roll

- Mold

- Rolling tool

- Forming tool

- Machining tool

- High performance cutting tools, stamping, woodworking, drawing, deep drawing and pressing tools, for ceramics and pharmaceutical industries, rolls, measuring tools, plastic moulds, shear blades.

Quality Assurance

Our D3 1.2080 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our D3 1.2080 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

SIZE RANGE

Products                             Diameter (mm)

Hot Rolled bar                       8 - 65

Forged and Turned bars        65.2 - 500

Forged Square Bars              50 - 500

FLATS

THICKNESS                     WIDTH

6.00 mm - 410.00 mm       20.00 mm  - 700.00 mm

Click here to contact our experienced sales team who will assist you with your D3 1.2080 tool steel enquiry.

3. O1 Steel Grade:

Grade Brief:

Toolman Special Steels is proud to produce and offer O1 (1.2510) - This alloy is one of the cold work, oil hardening type tool steels. It is relatively inexpensive containing small amounts of manganese, tungsten and chromium. Thanks to its tungsten and higher chromium content, the O1 tool steel has good wear resistance and polishing performance. O1 has good durability, wear resistance, and fine grain size. After heat treatment, it has very small dimensional variation. It is suitable for measurement tools and drills.

Steel Properties

- High wear resistance

- Fine grain size

- Good toughness

- Good durability

- High machinability,

- Medium toughness and resistance to wear.

- Dimensional stability during heat treatment.

- Good cutting edge retention

Specifications

Chemical Composition

| C | Si | Mn | P | S | Cr | V | W |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.85 - 1.00 | 0.10 - 0.50 | 1.00 - 1.40 | 0.03 | 0.03 | 0.4 - 0.7 | 0.15 - 0.30 | 0.40 - 0.60 |

Mechanical Properties:

| Property | Value |
| --- | --- |
| Annealing Hardness (HBW) | 212 max |
| Quenching and Tempering Hardness (HRC) | 59 min |

Physical Properties

| Property | Value |
| --- | --- |
| Density (g/cm³) | 7.7 |

Modulus of Elasticity

| Temperature (°C) | GPa |
| --- | --- |
| 20 | 193 |

Thermal Properties

Thermal Expansion Coefficient

| Temperature (°C) | Thermal Expansion Coefficient (10^-6/°C) |
| --- | --- |
| 20 - 260 | 10.6 |

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 20 | 33.4 |

HEAT TREATMENT AND PROCESSES

| Heat Treatment | Temperature | Duration | Cooling |
| --- | --- | --- | --- |
| Stress Relieving | Approx. 650 °C in the annealed state | 1 hour per 50 mm wall thickness | Furnace |
| Soft Annealing | 750 °C | 1 hour per 25 mm wall thickness | Furnace |
| Hardening | 830 °C | 1 minute per mm wall thickness |  |
| Quenching Hardness | Max. 64 HRC |  | in oil, hot bath or vacuum |
| Tempering | See tempering curve | 1 hour per 25 mm wall thickness | Air |
| Working Hardness | 58–62 HRC |  |  |

| Tempering °C after Quenching | 100 | 200 | 300 | 400 |
| --- | --- | --- | --- | --- |
| HRC | 64 | 62 | 57 | 53 |

Applications

- Blanking and stamping dies for cutting sheets up to 6 mm thickness

- Threading tools

- Drills

- Broaches

- Gauges, Measuring tools

- Plastic moulds

- Shear blades

- Guide rails

Quality Assurance

Our O1 1.2510 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our O1 1.2510 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

Products                             Diameter (mm)

Hot Rolled bar                       8 - 65

Forged and Turned bars        65.2 - 500

Forged Square Bars              50 - 500

FLATS

THICKNESS                     WIDTH

6.00 mm - 410.00 mm       20.00 mm  - 700.00 mm

Click here to contact our experienced sales team who will assist you with your O1 1.2510 tool steel enquiry.

4. S1 Steel Grade:

Grade Brief:

Toolman Special Steels is proud to produce and offer S1(1.2550) - AISI S1 is an impact resistant tool steel with extremely high toughness, and high hardenability. It can be used for tungsten alloy cold work tools. It is applied for cutting tools for plates, wood-working tool, and blanking dies.

Steel Properties

- High impact resistance

- Good wear resistance

- Good toughness with high strength

- High hardenability

- Shock resisting tool steel with very good toughness in combination with high hardenability.

Specifications

Chemical Composition

| C | Si | Mn | P | S | Cr | Mo | V | W |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0.40 - 0.55 | 0.15 - 1.20 | 0.10- 0.40 | 0.03 | 0.03 | 1.00- 1.80 | 0.00 - 0.50 | 0.15 - 0.30 | 1.50 - 3.00 |

Mechanical Properties:

| Property | Value |
| --- | --- |
| Annealing Hardness (HBW) | 229 max |
| Quenching and Tempering Hardness (HRC) | 56 min |

Physical Properties

| Property | Value |
| --- | --- |
| Density (g/cm³) | 7.86 |

Modulus of Elasticity

| Temperature (°C) | GPa |
| --- | --- |
| 20 | 190 |

Thermal Properties

Thermal Expansion Coefficient

| Temperature (°C) | Thermal Expansion Coefficient (10^-6/°C) |
| --- | --- |
| 20 - 100 | 12.4 |

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 20 | 41 |

HEAT TREATMENT AND PROCESSES

| Heat Treatment | Temperature | Duration | Cooling |
| --- | --- | --- | --- |
| Stress Relieving | Approx. 650 °C in the annealed state | 1 hour per 50 mm wall thickness | Furnace |
| Soft Annealing | 760 °C | 1 hour per 25 mm wall thickness | Furnace |
| Hardening | 890 °C | 1 minute per mm wall thickness |  |
| Quenching Hardness | Max. 60 HRC |  | in oil, hot bath or vacuum |
| Tempering | See tempering curve | 1 hour per 25 mm wall thickness | Air |
| Working Hardness | 58–62 HRC |  |  |

| Tempering °C after Quenching | 100 | 200 | 300 | 400 | 500 | 600 |
| --- | --- | --- | --- | --- | --- | --- |
| HRC | 60 | 58 | 56 | 52 | 48 | 43 |

Applications

- Blanking dies for cutting sheets up to 12 mm thickness

- Trimming and splitting dies

- Cold piercing punches

- Preforming punches

- Shear blades

- Chipping knives

- Pneumatic chisels

- Coining tools,

- Cold shear blades

- Ejectors

Quality Assurance

Our S1 1.2550 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our S1 1.2550 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

Products                             Diameter (mm)

Hot Rolled bar                       8 - 65

Forged and Turned bars        65.2 - 500

Forged Square Bars              50 - 500

FLATS

THICKNESS                     WIDTH

6.00 mm - 410.00 mm       20.00 mm  - 700.00 mm

Click here to contact our experienced sales team who will assist you with your S1 1.2550 tool steel enquiry.

5. A2 Steel Grade:

Grade Brief:

Toolman Special Steels is proud to produce and offer A2(1.2363) - This alloy is one of the cold work, medium air hardening type tool steels. It contains chromium and molybdenum with a relatively high (1 %) carbon content and is capable of deep hardening from air quench so as to minimise distortion. It can be hardened through air cooling. A2’s wear resistance lies between that of O1 and that of D2 tool steel so that it is suitable for common materials in many applications.

Steel Properties

- Proper combination of toughness and wear resistance

- High softening resistance

- Low deformation and high safety during heat treatment

- High harden-ability

- High dimensional stability during heat treatment

- High wear resistance and toughness.

Specifications

Chemical Composition

| Element | Min (%) | Max (%) |
| --- | --- | --- |
| C | 0.95 | 1.05 |
| Si | 0.10 | 0.50 |
| Mn | 0.40 | 1.00 |
| P | - | 0.030 |
| S | - | 0.030 |
| Cr | 4.75 | 5.5 |
| Mo | 0.90 | 1.40 |
| V | 0.15 | 0.50 |

Mechanical Properties:

| Property | Value |
| --- | --- |
| Annealing Hardness (HBW) | 231 max |
| Quenching and Tempering Hardness (HRC) | 60 min |

Physical Properties

| Property | Value |
| --- | --- |
| Density (g/cm³) | 7.7 |

Modulus of Elasticity

| Temperature (°C) | GPa |
| --- | --- |
| 20 | 190 |

Thermal Properties

Thermal Expansion Coefficient

| Temperature (°C) | Thermal Expansion Coefficient (10^-6/°C) |
| --- | --- |
| 400 | 11.6 |
| 500 | 11.7 |

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 20 | 26 |

HEAT TREATMENT AND PROCESSES

| Soft annealing °C | Cooling | Hardness HB |
| --- | --- | --- |
| 800 - 840 | Furnace | Max 231 |

| Stress-relief annealing °C | Cooling |
| --- | --- |
| approx. 650 | Furnace |

| Hardening °C | Quenching | Hardness after quenching HRC |
| --- | --- | --- |
| 930 – 970 | Air, oil saltbath 500 – 550 °C | 60 min |

| Tempering °C after Quenching | 100 | 200 | 300 | 400 | 500 | 600 |
| --- | --- | --- | --- | --- | --- | --- |
| HRC | 63 | 62 | 59 | 57 | 59 | 52 |

Applications

- Cutting tools

- Rolls

- Shear blades

- Cold pilger mandrels

- Cold stamping tools

- Moulds for plastics processing

- Used of die shapes, slitters, cutting, stamping, injection tools and similar applications where wear resistance is important

Quality Assurance

Our A2 1.2363 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our A2 1.2363 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

Products                             Diameter (mm)

Hot Rolled bar                       8 - 65

Forged and Turned bars        65.2 - 500

Forged Square Bars              50 - 500

FLATS

THICKNESS                     WIDTH

6.00 mm - 410.00 mm       20.00 mm  - 700.00 mm

Click here to contact our experienced sales team who will assist you with your A2 1.2363 tool steel enquiry.

6. 1.2767 Steel Grade:

Grade Brief:

Toolman Special Steels is proud to produce and offer 1.2767 steel. 1.2767 (45NiCrMo16) is a high-carbon, high-chromium tool steel that contains nickel for enhanced toughness. It is known for its excellent toughness and good wear resistance, making it suitable for high-impact applications. This nickel containing cold work tool steel has good hardenability and toughness, and can be polished, photo-etched, and etched. It is applied for forged tools, molds of various shapes and dimensions, and hot forged as well as stamping tools.

Steel Properties

- Good hardenability

- Dimensionally stable steel with high toughness and resistance to impact and compressive stress.

- High impact resistance

- Good wear resistance

- High Compressive strength

- Proper machinability

- Ability for polishing, photo-etching and erosion treatment

Specifications

Chemical Composition

| Element | Min (%) | Max (%) |
| --- | --- | --- |
| C | 0.40 | 0.50 |
| Si | 0.10 | 0.40 |
| Mn | 0.15 | 0.45 |
| P | - | 0.030 |
| S | - | 0.030 |
| Cr | 1.20 | 1.50 |
| Mo | 0.15 | 0.35 |
| Ni | 3.80 | 4.30 |

Mechanical Properties:

| Property | Value |
| --- | --- |
| Annealing Hardness (HBW) | 262 max |
| Quenching and Tempering Hardness (HRC) | 52 min |

Physical Properties

| Property | Value |
| --- | --- |
| Density (g/cm³) | 7.84 |

Modulus of Elasticity

| Temperature (°C) | GPa |
| --- | --- |
| 20 | 190 |

Thermal Properties

Thermal Expansion Coefficient

| Temperature (°C) | Thermal Expansion Coefficient (10^-6/°C) |
| --- | --- |
| 20 - 100 | 11.7 |

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 20 | 28 |

HEAT TREATMENT CONDITIONS REMOVE HEAT TREATMENT DATA FROM DATASHEET PDF)

HEAT TREATMENT CONDITIONS

850℃ Oil Cooling +180℃ Air Cooling

| Tempering °C after Quenching | 100 | 200 | 300 | 400 | 500 | 600 | 700 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| HRC | 57 | 56 | 51 | 48 | 44 | 40 | 38 |

Applications

- Mould plates and inserts for the processing of thermoplastics and thermosets, especially for high gloss polishes, e.g. for transparent melts and components with high surface requirements, mould components with high compressive and flexural stresses, embossing tools and other uses for which the above requirements are needed.

- Cutlery dies

- Cutting tools for thick material

- Billet-shear blades

- Drawing jaws

- Massive embossing and bending tools,

- Plastic moulds, reinforcements.

- Stamping tool

Quality Assurance

Our 1.2767 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our 1.2767 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

Products                             Diameter (mm)

Hot Rolled bar                       8 - 65

Forged and Turned bars        65.2 - 500

Forged Square Bars              50 - 500

FLATS

THICKNESS                     WIDTH

6.00 mm - 410.00 mm       20.00 mm  - 700.00 mm

Click here to contact our experienced sales team who will assist you with your 1.2767 tool steel enquiry.

7. D2 1.2601 Steel Grade:

Grade Brief:

Toolman Special Steels is proud to produce and offer 1.2601 steel. It is a Ledeburitic Cr-steel and corresponds to material number 1.2601 (X165CrMoV12). This alloy possesses a very high compressive strength and is deep hardening. 1.2601 steel is designed for high-performance cutting tools. It offers superior toughness compared to D3 steel and can be nitrided to enhance surface hardness and wear resistance.

Steel Properties

- Wear resistance

- Compressive Strength

Specifications

Chemical Composition (PLEASE CHANGE THE COMPOSITION ON DATA SHEET PROVIDED IN PDF AS PER BELOW COMPOSITION) - ALSO REMOVE THE FORGING, MACHINABILITY AND DISCLAIMER PORTION IN THE DATA SHEET )

| C | Si | Mn | P | S | Cr | Mo | V | W |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1.60 | 0.35 | 0.30 | 0.03 | 0.03 | 11.50 | 0.60 | 0.30 | 0.50 |

Mechanical Properties:

| Property | Value |
| --- | --- |
| Annealing Hardness (HB) | 250 max |
| Tensile Strength | 1500-2000 MPa |
| Yield Strength | 1300-1800 MPa |

Physical Properties

| Property | Value |
| --- | --- |
| Density (g/cm³) | 7.70 |

Modulus of Elasticity

| Temperature (°C) | GPa |
| --- | --- |
| 20 | 210 |

Thermal Properties

Thermal Expansion Coefficient

| Temperature (°C) | Thermal Expansion Coefficient (10^-6/°C) |
| --- | --- |
| 20 - 100 | 10.5 |

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 20 | 20 |

HEAT TREATMENT AND PROCESSES

| Process | Description | Temperature Range | Cooling Method | Resulting Hardness |
| --- | --- | --- | --- | --- |
| Soft Annealing | Heating to 800-840°C followed by slow cooling in a furnace. This relieves internal stresses and produces a maximum Brinell hardness of 255. | 800-840°C | Slow furnace cooling | Maximum 255 Brinell |
| Stress Relieving | Heating to 650°C, holding for one hour, then air cooling. This process is done to relieve machining stresses and reduce distortion during heat treatment. | 650°C | Air cooling | - |
| Hardening | Heating to 980-1010°C followed by quenching in oil, air, or warm bath. This process increases hardness (63-65 HRC) by transforming the material's structure. | 980-1010°C | Oil, air, or warm bath quenching | 63-65 HRC |
| Tempering | Heating to 150-400°C. This process follows hardening and reduces brittleness, increasing toughness and ductility while maintaining some hardness. | 150-400°C | - | - |

| Tempering °C after Quenching | 100 | 200 | 300 | 400 |
| --- | --- | --- | --- | --- |
| HRC | 64 | 62 | 60 | 58 |

Applications

- Machine knife (for producers)

- Rolling Cold Forming

- Fine Blanking, Stamping, Blanking Standard Parts (Molds, Plates, Pins, Punches)

- Components for Recycling Industry

- Rolls Wear parts

- General Components for Mechanical Engineering

- Cutting tools, stamping, woodworking, drawing, deep drawing and pressing tools, cold working rolls, measuring tools.

Quality Assurance

Our D2 M 1.2601 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our 1.2601 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

Products                             Diameter (mm)

Hot Rolled bar                       8 - 65

Forged and Turned bars        65.2 - 500

Forged Square Bars              50 - 500

FLATS

THICKNESS                     WIDTH

6.00 mm - 410.00 mm       20.00 mm  - 700.00 mm

Click here to contact our experienced sales team who will assist you with your D2 M 1.2601 tool steel enquiry.

8. S7 1.2357 Steel Grade:  (NOTE - REMOVE 3RD PAGE FROM DATA SHEET PROVIDED IN PDF)

Grade Brief:

Toolman Special Steels is proud to produce and offer S7 1.2357 steel. S7 is a general purpose air hardening tool steel having high impact and sock resistance. This steel product has a special property combination of high impact resistance and toughness. It can be easily processed and heat treated. It has good softening resistance at medium temperatures and often used in the shock resisting applications.

Steel Properties

- High impact resistance

- Good wear resistance

- Good toughness with high strength

- High hardenability

- Softening resistance

- Good Polishability

Specifications

Chemical Composition

| Element | Min (%) | Max (%) |
| --- | --- | --- |
| C | 0.45 | 0.55 |
| Si | 0.20 | 1.00 |
| Mn | 0.20 | 0.90 |
| P | - | 0.030 |
| S | - | 0.030 |
| Cr | 3.00 | 3.50 |
| Mo | 1.30 | 1.80 |
| V | 0.00 | 0.35 |

Mechanical Properties:

| Property | Value |
| --- | --- |
| Annealing Hardness (HBW) | 229 max |
| Quenching and Tempering Hardness (HRC) | 56 min |

Physical Properties

| Property | Value |
| --- | --- |
| Density (g/cm³) | 7.76 |

Modulus of Elasticity

| Temperature (°C) | GPa |
| --- | --- |
| 20 | 210 |

Thermal Properties

Thermal Expansion Coefficient

| Temperature (°C) | Thermal Expansion Coefficient (10^-6/°C) |
| --- | --- |
| 400 | 13.8 |
| 500 | 14.1 |

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 20 | 28.5 |

HEAT TREATMENT AND PROCESSES (EDIT HARDNESS TO 229 IN DATASHEET)

| Soft annealing °F | Cooling | Hardness HB |
| --- | --- | --- |
| 1130 - 1200 | Furnace 20°F/hr to | Max 229 |
|  | 930°F then air cool |  |

| Stress-relief annealing | Temperature and Cooling |
| --- | --- |
| Annealed Parts | 1200°F - 1250°F Hold time 2 hours, slowly cool to 930°F, then air cool |
| Hardened Parts | Heat to 25°F - 50°F below the original tempering temperature, hold for 2 hours, then cool in air |

| Hardening °F | Quenching | Hardness after quenching HRC |
| --- | --- | --- |
| 1690°F - 1775°F Hold at temperature for 30 minutes | Furnace quench to 350°F, air cool to 120°F. Immediately temper | 60 - 62 |

| Tempering °C after Quenching | 100 | 200 | 300 | 400 | 500 | 600 |
| --- | --- | --- | --- | --- | --- | --- |
| HRC | 60 | 58 | 54 | 53 | 53 | 44 |

Applications

- Compression molds

- Tablet compression dies

- Injection mold

- Shears

- Blanking dies

- Punches

- Chisels

- Rivet sets

- Driver bolts

Quality Assurance

Our S7 1.2357 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our S7 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

Products                             Diameter (mm)

Hot Rolled bar                       8 - 65

Forged and Turned bars        65.2 - 500

Forged Square Bars              50 - 500

FLATS

THICKNESS                     WIDTH

6.00 mm - 410.00 mm       20.00 mm  - 700.00 mm

Click here to contact our experienced sales team who will assist you with your S7 1.2357 tool steel enquiry.

9. A8 M Steel Grade: (Remove shape section in the data sheet provided in pdf form)

Grade Brief:

Toolman Special Steels is proud to produce and offer A8 M Steel. AISI A8 is premium medium carbon high Cr, Mo, V alloy tool steel. When compared to D2 with a high carbon and chromium content, A8 has higher toughness. It also has better wear resistance than shock-resisting steel, such as S7 so that it is the best choice for the applications that require high strength and high mold.

Steel Properties

- Good cutting ability

- High hardenability

- High surface strength

- Easy to repair and weld

- High cutting power, high wear resistance as well as excellent tempering resistance.

Specifications

Chemical Composition (EDIT THE VALUES OF THE COMPOSITION IN THE DATSHEET PDF PROVIDED TO YOU AS PER BELOW RANGE)

| C | Si | Mn | Cr | Mo | V |
| --- | --- | --- | --- | --- | --- |
| 0.52 | 0.95 | 0.40 | 8.00 | 1.40 | 0.45 |

Mechanical Properties:

| Property | Value |
| --- | --- |
| Annealing Hardness (HBW) | 250 max |
| Quenching and Tempering Hardness (HRC) | 56 min |
| Tensile strength Rm (as received condition) | 123.2 KSI |

Physical Properties

| Property | Value |
| --- | --- |
| Density (g/cm³) | 7.75 |

Modulus of Elasticity

| Temperature (°C) | GPa |
| --- | --- |
| 20 | 200 |

Thermal Properties

Thermal Expansion Coefficient

| Temperature (°C) | Thermal Expansion Coefficient (10^-6/°C) |
| --- | --- |
| 20 - 200 | 11.6 |

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 20 | 26.1 |

HEAT TREATMENT AND PROCESSES

| Soft annealing °F | Cooling | Hardness HB |
| --- | --- | --- |
| 1526 - 1580°F | Furnace | Max 250 |

| Stress-relief annealing °F | Cooling |
| --- | --- |
| approx. 1202°F | Furnace |

| Hardening °F | Quenching | Hardness after quenching HRC |
| --- | --- | --- |
| 1886 - 1958°F | Air, oil, hot basin (1022°F) | 56 min |

| Tempering °C after Quenching | 100 | 200 | 300 | 400 | 500 | 550 | 600 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| HRC | 61 | 60 | 58 | 58 | 60 | 57 | 53 |

Applications

- Applications severely stressed machine blades for cellulose and paper industries

- Woodworking milling cutters, flat and circular blades for cutting 5 to 15 mm thick sheet/plate.

- Blanking tools, stamping tools, embossing tools, forming dies, press dies, die inserts

- Extrusion dies, reinforcements, cold extrusion tools, tube tools, cutting tools, industrial knives, wood chipping knives, veneer knives

Quality Assurance

Our A8 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our A8 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

Products                             Diameter (mm)

Hot Rolled bar                       8 - 65

Forged and Turned bars        65.2 - 500

Forged Square Bars              50 - 500

FLATS

THICKNESS                     WIDTH

6.00 mm - 410.00 mm       20.00 mm  - 700.00 mm

Click here to contact our experienced sales team who will assist you with your A8 tool steel enquiry.

10. DC 53:

Grade Brief:

Toolman Special Steels is proud to produce and offer DC 53 Steel. DC-53 is a general purpose cold work tool steel with exceptional Toughness, Wear Resistance, Compressive Strength and Temper Resistance. DC53, is an improvement over alloy tool steel D-2. It eliminates the disadvantages of insufficient hardness and toughness. DC53 steel also has excellent machining characteristics and is well suited as a substrate for PVD surface treatments

Steel Properties

- Higher hardness (62-63HRc) than D2 after heat treatment

- Twice the toughness of D2 with a superior wear resistance

- 20% higher fatigue strength than D2

- Smaller primary carbides than D2 protect the die from chipping and cracking

- Machines and grinds up to 40% faster than D2

Specifications

Chemical Composition

| C | Si | Mn | Cr | Mo | V |
| --- | --- | --- | --- | --- | --- |
| 0.95 | 1.00 | 0.30 | 8.00 | 2.10 | 0.30 |

Mechanical Properties:

| Property | Value |
| --- | --- |
| Quenching and Tempering Hardness (HRC) | 61 - 63 |
| Poisson’s ratio (25°C) | 0.31 |
| Rigidity Modulus | 79 Gpa |
| Tensile Strength | 2200 MPa |

Physical Properties

| Property | Value |
| --- | --- |
| Density (g/cm³) | 7.70 |

Modulus of Elasticity

| Temperature (°C) | GPa |
| --- | --- |
| 20 | 210 |

Thermal Properties

Thermal Expansion Coefficient

| Temperature (°C) | Thermal Expansion Coefficient (10^-6/°C) |
| --- | --- |
| 20 - 200 | 11.6 |

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 20 | 20 |

HEAT TREATMENT AND PROCESSES

| Soft annealing °C | Cooling | Hardness HB |
| --- | --- | --- |
| 830 - 880 | Furnace | Max 255 |

| Stress-relief annealing °C | Cooling |
| --- | --- |
| approx. 600 | Furnace |

| Hardening °C | Quenching | Hardness after quenching HRC |
| --- | --- | --- |
| 1020 - 1040 | Oil, air, or vacuum quenching | 62 -64 |

Tempering

| Process | Details |
| --- | --- |
| Tempering | Perform in non-atmosphere controlled convection furnace. First temper at 45-65°C. Allow to cool to ambient temperature between tempers. |

Applications

- Blanking Dies

- Progressing Dies, Rolling Dies, Bending Dies

- Cold Forging Dies, Drawing Dies

- Rolls

- Punches

- Plastic Molds

- Trimming Dies

- Shear Blades

- Stripper plates for lead frame blanking

- Gauges

- Screws for injection molding machines

Quality Assurance

Our DC 53 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our DC 53 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

Products                             Diameter (mm)

Hot Rolled bar                       8 - 65

Forged and Turned bars        65.2 - 500

Forged Square Bars              50 - 500

FLATS

THICKNESS                     WIDTH

6.00 mm - 410.00 mm       20.00 mm  - 700.00 mm

Click here to contact our experienced sales team who will assist you with your DC 53 tool steel enquiry.