Notes :

- The composition of the grades present in this PDF is accurate. The data sheets provided to you as a separate attachment - kindly edit the values of the composition there as per this sheet. In form supplied column given in data sheet - only round bars, square bars and flat bars needed - rest pls remove.

- This is the required content. Kindly present according to the website colour scheme. Wherever necessary, provide the details in tabular form such as chemical composition, size ranges etc (in whatever way it looks good).

- If form of supply is mentioned in the data sheet - only keep round, squares and flats. Rest remove. AND wherever NOTE IS WRITTEN - kindly go through that instruction.

1. M2 Steel Grade:

Grade Brief:

Toolman Special Steels is proud to produce and offer M2 (1.3343) - a medium alloy high speed steel with good machinability. The M2 alloy has somewhat better wear resistance than M1. In addition, it achieves a balance between toughness, wear resistance, and thermal hardness because of its alloy composition. It is widely used for cutting tools and other applications requiring high-performance materials.

STANDARDS (NOTE : PLEASE SEE HOW YOU CAN PRESENT THIS WHETHER YOU WANT TO PRESENT WITH CHEMICAL COMPOSITION OR ANYTHING ELSE)

Europe : HS 6-5-2

Sweden : SS 2722

Japan : JIS SKH51

Germany : 1.3343

USA : AISI M2

Steel Properties

- Outstanding cutting hardness, wear resistance, and toughness at high temperatures

- Special carbide precipitated during tempering at high temperatures and secondary hardening

- Fine grain size

- Uniform carbide

- High toughness

- Good toughness and cutting capability

- Deep hardening response.

Specifications

Chemical Composition (PLEASE EDIT THESE VALUES IN THE DATA-SHEET PROVIDED IN THE PDF.. ALSO, REPLACE E- M2 WITH JUST M2 IN DATA-SHEET)

| C | Cr | Mo | W | Co | V |
| --- | --- | --- | --- | --- | --- |
| 0.9 | 4.1 | 5.00 | 6.00 | - | 1.8 |

Mechanical Properties:

| Property | Value |
| --- | --- |
| Hardness (HBW) | 250 max (Annealed) |
| Quenching and Tempering Hardness (HRC) | 64 min |

Physical Properties

| Property | Value |
| --- | --- |
| Density (g/cm³) | 8.1 |

Modulus of Elasticity

| Temperature (°C) | kN/mm² |
| --- | --- |
| 20 | 225 |

Thermal Properties

Thermal Expansion Coefficient

| Temperature (°C) | Thermal Expansion Coefficient (10^-6/°C) |
| --- | --- |
| 400 | 12.1 |
| 600 | 12.6 |

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 20 | 24 |
| 400 | 28 |
| 600 | 27 |

HEAT TREATMENT AND PROCESSES

| Heat Treatment Process | Temperature Range | Procedure | Purpose | Resulting Hardness (HRC) |
| --- | --- | --- | --- | --- |
| Annealing | 850-880°C | Heat slowly to 850-880°C, hold until uniform, cool in the furnace to room temperature | To soften the steel and relieve internal stresses | - |
| Stress Relieving | 600-700°C | Heat to 600-700°C, hold until uniform, cool in still air | To remove machining stresses | - |
| Hardening | 1200-1250°C | Preheat to 450-500°C, then heat rapidly to 1200-1250°C, hold until uniform, quench in oil or air | To increase hardness and wear resistance | - |
| Tempering | 540-600°C | Heat to 540-600°C, hold for at least 2 hours, cool in still air | To balance hardness, strength, and toughness | 58-65 HRC |

Applications

- Knives, thread cutting and twist drills

- Broaching and milling tools, woodworking tools, cold working tools

- Sendizimir rolls

- Reamers circular saw segments

- Cold forming like cold extrusion rams and dies

- Plastic moulds with elevated wear resistance and screws

- Mold applicaitons (screw mold, header punch, die)

Quality Assurance

Our M2 1.3343 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our M2 1.3343 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

| ROUNDS |  | SQUARES |  |
| --- | --- | --- | --- |
| SIZE (MM) | CONDITION | SIZE (MM) | CONDITION |
| 6.00 - 14.00 | CG | 7.2, 8.8, 10.5, 11 | HRA |
| 15.00 - 50.00 | HRAP | 13.5, 14, 17.5, 21 | HRA |
| 52.00 - 405.00 | FAT | 27, 32, 40 | HRA |
|  |  | 52.00 - 305.00 | FA |

| FLATS |  |  |  |
| --- | --- | --- | --- |
| THICKNESS (MM) | WIDTH (MM) | CONDITION |  |
| 5.00 - 32.00 | 21.00 - 105.00 | HRA |  |
| 32.00 - 105.00 | 40.00 - 205.00 | FA |  |

Click here to contact our experienced sales team who will assist you with your M2 1.3343 tool steel enquiry.

2. M3 Steel Grade:

Grade Brief:

Toolman Special Steels is proud to produce and offer M3 (1.3344) -  a highly alloyed high speed steel for good wear resistance and high hardness. M3 Type II is a tungsten molybdenum high speed tool steel designed to provide the great wear resistance required for severe cutting operations with a raised C and V content. It is used for high performance mills, reamers, broaches for processing hard materials as well as in the area of cold work steel e.g. for piercing dies in the manufacture of nuts.

STANDARDS (NOTE : PLEASE SEE HOW YOU CAN PRESENT THIS WHETHER YOU WANT TO PRESENT WITH CHEMICAL COMPOSITION OR ANYTHING ELSE)

- Europe : HS 6-5-3

- Sweden : SS2785

- Japan : JIS SKH53

- Germany : 1.3344

- USA : AISI M3:2

Steel Properties

- Molybdenum high - speed tool steel.

- Basic chemical composition as M2, with higher V- and C- content

- Very high resistance to wear and to softening

- High resistance of blade and good toughness

- Deep hardening response.

Specifications

Chemical Composition (PLEASE EDIT THESE VALUES IN THE DATA-SHEET PROVIDED IN THE PDF.. (ALSO REMOVE RAVNE IN DATASHEET)

| C | Cr | Mo | W | Co | V |
| --- | --- | --- | --- | --- | --- |
| 1.20 | 4.30 | 5.10 | 6.40 | - | 3.30 |

Mechanical Properties:

| Property | Value |
| --- | --- |
| Hardness (HBW) | 280 max (Annealed) |
| Quenching and Tempering Hardness (HRC) | 64 min |

Physical Properties

| Property | Value |
| --- | --- |
| Density (g/cm³) | 8.07 |

Modulus of Elasticity

| Temperature (°C) | 10³N/mm² |
| --- | --- |
| 20 | 217 |

Thermal Properties

Thermal Expansion Coefficient

| Temperature (°C) | Thermal Expansion Coefficient (10^-6/°C) |
| --- | --- |
| 400 | 12.8 |
| 600 | 13 |

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 20 | 19 |

HEAT TREATMENT AND PROCESSES

| Process | Steps | Temperature | Details | Resulting Hardness |
| --- | --- | --- | --- | --- |
| Soft Annealing | Heat | 820-860°C | Cool slowly in furnace | Max Brinell hardness of 280 |
| Hardening | 1st Pre-heating | 400°C |  |  |
|  | 2nd Pre-heating | 850°C |  |  |
|  | 3rd Pre-heating | 850°C and 1050°C |  |  |
|  | Harden | 1190-1300°C | Oil or air quenching, or warm bath at 550°C/air |  |
| Tempering | Temper | 540-570°C | At least 3 times | Hardness of 64-66 HR |

| Tempering °C after quenching | 200 | 300 | 400 | 500 | 525 | 550 | 600 | 700 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| HRC | 63 | 61 | 61.5 | 63 | 65 | 65.5 | 63 | 47 |

Applications

- Tap drills

- Reamers

- Heavy duty milling cutters

- Dies

- Broach needles hexagon socket punches

- Piercing dies for nut production

Quality Assurance

Our M3 1.3344 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our M3 1.3344 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

| ROUNDS |  | SQUARES |  |
| --- | --- | --- | --- |
| SIZE (MM) | CONDITION | SIZE (MM) | CONDITION |
| 6.00 - 14.00 | CG | 7.2, 8.8, 10.5, 11 | HRA |
| 15.00 - 50.00 | HRAP | 13.5, 14, 17.5, 21 | HRA |
| 52.00 - 405.00 | FAT | 27, 32, 40 | HRA |
|  |  | 52.00 - 305.00 | FA |

| FLATS |  |  |  |
| --- | --- | --- | --- |
| THICKNESS (MM) | WIDTH (MM) | CONDITION |  |
| 5.00 - 32.00 | 21.00 - 105.00 | HRA |  |
| 32.00 - 105.00 | 40.00 - 205.00 | FA |  |

Click here to contact our experienced sales team who will assist you with your M3 1.3344 tool steel enquiry.

3. M7 Steel Grade:

Grade Brief:

Toolman Special Steels is proud to produce and offer M7 (1.3348) - M7 is one of the molybdenum alloy high speed tool steels and contains tungsten, chromium and vanadium for better strength. It has good hardenability and superior wear resistance. M7 is widely used in the cutting tools, cutting drills, and cold forming tools for machining operations.

STANDARDS (NOTE : PLEASE SEE HOW YOU CAN PRESENT THIS WHETHER YOU WANT TO PRESENT WITH CHEMICAL COMPOSITION OR ANYTHING ELSE)

- Europe : HS 2-9-2

- Sweden : SS2782

- Japan : JIS SKH58

- Germany : 1.3348

- USA : AISI M7

Steel Properties

- High hardness after quenching and tempering

- High wear resistance and cutting ability

- Good grindability

- High impact resistance

- Edge Stability

Specifications

Chemical Composition (PLEASE EDIT THESE VALUES IN THE DATA-SHEET PROVIDED IN THE PDF.. ALSO, REPLACE E- M2 WITH JUST M2 IN DATA-SHEET)

| C | Cr | Mo | W | Co | V |
| --- | --- | --- | --- | --- | --- |
| 0.97 | 3.00 | 8.20 | 1.40 | - | 1.75 |

Mechanical Properties:

| Property | Value |
| --- | --- |
| Hardness (HBW) | 255 max (Annealed) |
| Quenching and Tempering Hardness (HRC) | 65 min |

Physical Properties

| Property | Value |
| --- | --- |
| Density (g/cm³) | 7.9 |

Modulus of Elasticity

| Temperature (°C) | Gpa |
| --- | --- |
| 20 | 217 |

Thermal Properties

Thermal Expansion Coefficient

| Temperature (°C) | Thermal Expansion Coefficient (10^-6/°C) |
| --- | --- |
| 20 - 100 | 11.7 |
| 20 - 500 | 13.4 |

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 20 | 19 |

HEAT TREATMENT AND PROCESSES

| Heat Treatment Process | Temperature (°C) | Details |
| --- | --- | --- |
| Annealing | 850-900 | Heat uniformly, hold until soaked, cool slowly in furnace. |
| Stress Relieving | 600-700 | Heat to specified temperature, hold for 2 hours, then air cool. |
| Hardening (Step 1) | 450 - 500 | Preheat uniformly, hold until soaked. |
| Hardening (Step 2) | 850 - 900 | Heat uniformly, hold until soaked, quench in oil, salt bath, or air. Austenitise at a temperature suitable for chosen working hardness. |
| Tempering | 540-600 | Reheat, hold for at least one hour per inch of thickness, air cool. |

Applications

- Cutting tools in machining operations

- Sendzimir rolls

- Segment and circular cutters

- Profile cutting tools

- Thread cutting drills

- Cold forming tools

- Cold forming mold (screw mold, header punch, die)

Quality Assurance

Our M7 1.3348 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our M7 1.3348 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

| ROUNDS |  | SQUARES |  |
| --- | --- | --- | --- |
| SIZE (MM) | CONDITION | SIZE (MM) | CONDITION |
| 6.00 - 14.00 | CG | 7.2, 8.8, 10.5, 11 | HRA |
| 15.00 - 50.00 | HRAP | 13.5, 14, 17.5, 21 | HRA |
| 52.00 - 405.00 | FAT | 27, 32, 40 | HRA |
|  |  | 52.00 - 305.00 | FA |

| FLATS |  |  |  |
| --- | --- | --- | --- |
| THICKNESS (MM) | WIDTH (MM) | CONDITION |  |
| 5.00 - 32.00 | 21.00 - 105.00 | HRA |  |
| 32.00 - 105.00 | 40.00 - 205.00 | FA |  |

Click here to contact our experienced sales team who will assist you with your M7 1.3348 tool steel enquiry.

4. M35 Steel Grade:

Grade Brief:

Toolman Special Steels is proud to produce and offer M35 (1.3243). It is medium alloy high speed steel and has better thermal hardness and wear resistance with better machinability than M2, because cobalt is added to it. . It features a strong cutting edge with good toughness, a deep hardening response, and maintains high hot hardness properties.

STANDARDS (NOTE : PLEASE SEE HOW YOU CAN PRESENT THIS WHETHER YOU WANT TO PRESENT WITH CHEMICAL COMPOSITION OR ANYTHING ELSE)

- Europe : HS 6-5-2-5

- Sweden : SS2723

- Japan : JIS SKH55

- Germany : 1.3243

- USA : AISI M35

Steel Properties

- Good high temperature hardness

- High wear resistance

- High cutting ability

- Fine and uniform grain size

- High resistance of cutting edge and good toughness.

- Good machinability

Specifications

Chemical Composition (PLEASE EDIT THESE VALUES IN THE DATA-SHEET PROVIDED IN THE PDF..)

| C | Cr | Mo | W | Co | V |
| --- | --- | --- | --- | --- | --- |
| 0.92 | 4.10 | 5.00 | 6.00 | 4.80 | 1.90 |

Mechanical Properties:

| Property | Value |
| --- | --- |
| Hardness (HBW) | 268 max (Annealed) |
| Quenching and Tempering Hardness (HRC) | 64 min |
| Tensile Strength (N/mm²) | 980 max |

Physical Properties

| Property | Value |
| --- | --- |
| Density (g/cm³) | 8.1 |

Modulus of Elasticity

| Temperature (°C) | 10^3 x (N/mm²) |
| --- | --- |
| 20 | 217 |

Thermal Properties

Thermal Expansion Coefficient

| Temperature (°C) | Thermal Expansion Coefficient (10^-6/°C) |
| --- | --- |
| 500 | 12.7 |
| 600 | 13 |

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 20 | 19 |

HEAT TREATMENT AND PROCESSES

| Heat Treatment Process | Temperature (°C) | Details | Resulting Hardness |
| --- | --- | --- | --- |
| Soft Annealing | 820-880 | Heat uniformly, hold until soaked, cool slowly in furnace. | Brinell hardness of 230-300 HB |
| Stress Relieving | 650 - 700 | Heat to specified temperature, hold for 1 hour, air cool. Reduces machining stresses to minimize distortion during further heat treatment. |  |
| Hardening | Step 1: 450-600 Step 2: 850 Step 3: 1050 Step 4: 1210-1250 | Preheat to 450-600, then to 850, and finally to 1050. Harden from 1210-1250 followed by oil, air quenching, or warm bath at 550. | 64-66 HRC after quenching |
| Tempering | 540-570 | Reheat to specified temperature, hold for 1 hour (repeat 3 times). |  |

| Tempering °C after quenching | 200 | 300 | 400 | 500 | 525 | 550 | 575 | 600 | 650 | 700 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| HRC | 63 | 61 | 62 | 64 | 64.5 | 65 | 64 | 63 | 55 | 46 |

Applications

- Broaches and Reamers

- End Mills Gear Cutting

- Shaving and Shaping Tools

- Twist Drills and Taps

- Special Cutting Tools

- Blades for Sawing Machines

- Profile Cutting Tools

Quality Assurance

Our M35 1.3243 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our M35 1.3243 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

| ROUNDS |  | SQUARES |  |
| --- | --- | --- | --- |
| SIZE (MM) | CONDITION | SIZE (MM) | CONDITION |
| 6.00 - 14.00 | CG | 7.2, 8.8, 10.5, 11 | HRA |
| 15.00 - 50.00 | HRAP | 13.5, 14, 17.5, 21 | HRA |
| 52.00 - 405.00 | FAT | 27, 32, 40 | HRA |
|  |  | 52.00 - 305.00 | FA |

| FLATS |  |  |  |
| --- | --- | --- | --- |
| THICKNESS (MM) | WIDTH (MM) | CONDITION |  |
| 5.00 - 32.00 | 21.00 - 105.00 | HRA |  |
| 32.00 - 105.00 | 40.00 - 205.00 | FA |  |

Click here to contact our experienced sales team who will assist you with your M35 1.3243 tool steel enquiry.

5. M42 Steel Grade: (NOTE : - ONLY KEEP FIRST 2 PAGES FROM DATA-SHEET FOR THIS GRADE AND REMOVE CARTECH WHEREVER IT IS MENTIONED)

Grade Brief:

Toolman Special Steels is proud to produce and offer M42 (1.3247) - a high speed cobalt alloy steel that is regularly manufactured. When compared to traditional high speed steel, it has outstanding thermal hardness so that it is suitable for higher cutting speeds or extends the time before the cutting tool needs replacement.

STANDARDS (NOTE : PLEASE SEE HOW YOU CAN PRESENT THIS WHETHER YOU WANT TO PRESENT WITH CHEMICAL COMPOSITION OR ANYTHING ELSE)

- Europe : HS 2-9-1-8

- Sweden : SS2723

- Japan : JIS SKH59

- Germany : 1.3247

- USA : AISI M42

Steel Properties

- Good high temperature hardness

- High wear resistance

- High cutting ability

- High impact resistance

- Fine and uniform grain size

- Good grindability due to lower V - content.

Specifications

Chemical Composition (PLEASE EDIT THESE VALUES IN THE DATA-SHEET PROVIDED IN THE PDF.. Also remove CARTECH wherever it is mentioned)

| C | Cr | Mo | W | Co | V |
| --- | --- | --- | --- | --- | --- |
| 1.10 | 3.90 | 9.20 | 1.40 | 7.80 | 1.20 |

Mechanical Properties:

| Property | Value |
| --- | --- |
| Hardness (HBW) | 269 max (Annealed) |
| Quenching and Tempering Hardness (HRC) | 66 min |

Physical Properties

| Property | Value |
| --- | --- |
| Density (g/cm³) | 8.3 |

Modulus of Elasticity

| Temperature (°C) | 10^3 x (N/mm²) |
| --- | --- |
| 20 | 225 |

Thermal Properties

Thermal Expansion Coefficient

| Temperature (°C) | Thermal Expansion Coefficient (10^-6/°C) |
| --- | --- |
| 500 | 12.4 |
| 600 | 12.5 |

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 20 | 19 |

HEAT TREATMENT AND PROCESSES

| Process | Details |
| --- | --- |
| Decarburization | Use rectified salt baths or proper atmosphere control in furnace hardening to avoid decarburization. |
| Normalizing | Not recommended. |
| Annealing | Pack in a container with a neutral packing compound or in a protective atmosphere. Heat uniformly to 1550/1600°F (843/871°C). Cool slowly in the furnace at a rate not exceeding 40°F (22°C) per hour to 1000°F (538°C), then cool naturally. Resulting hardness: BHN 255 or less. |
| Hardening | Preheat at 1500/1600°F (816/871°C) thoroughly. Transfer to high heat of 2150/2200°F (1177/1204°C) in salt or 25°F (14°C) higher in atmosphere furnaces.Quench in salt at 1000/1150°F (538/621°C) until equalised, then cool in air. Alternatively, quench in warm oil. Cool to 150°F (66°C) max before tempering. |
| Deformation | Size change is minimal during hardening. When hardened from 2175°F (1191°C) in salt, a 1" (25.4 mm) cube expands about 0.0005" (0.013 mm). Expands similarly when tempered at 1000°F (538°C). |
| Tempering | Temper between 950°F (510°C) and 1100°F (593°C). Tempering below 1000°F (538°C) not recommended. Use triple temper cycle with a minimum of two hours at temperature each time. Cool to room temperature after each cycle. |

| Tempering °C after quenching | 200 | 300 | 400 | 500 | 520 | 560 | 600 | 650 | 700 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| HRC | 62.5 | 61 | 61.5 | 66.5 | 68 | 67 | 64 | 50 | 42 |

Applications

- Drills

- Hobs

- Taps

- End mills

- Milling cutters

- Form and gear Cutters

- Broaches and Chasers

- Counterbores

- Trimming Dies

Quality Assurance

Our M42 1.3247 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our M42 1.3247 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

| ROUNDS |  | SQUARES |  |
| --- | --- | --- | --- |
| SIZE (MM) | CONDITION | SIZE (MM) | CONDITION |
| 6.00 - 14.00 | CG | 7.2, 8.8, 10.5, 11 | HRA |
| 15.00 - 50.00 | HRAP | 13.5, 14, 17.5, 21 | HRA |
| 52.00 - 405.00 | FAT | 27, 32, 40 | HRA |
|  |  | 52.00 - 305.00 | FA |

| FLATS |  |  |  |
| --- | --- | --- | --- |
| THICKNESS (MM) | WIDTH (MM) | CONDITION |  |
| 5.00 - 32.00 | 21.00 - 105.00 | HRA |  |
| 32.00 - 105.00 | 40.00 - 205.00 | FA |  |

Click here to contact our experienced sales team who will assist you with your M42 1.3247 tool steel enquiry.

6. ABC III Steel Grade:

Grade Brief:

Toolman Special Steels is proud to produce and offer ABC III(1.3333) - a medium alloyed high speed steel with good wear resistance. This economical high-speed steel is ideal for medium lifetimes, offering high toughness properties. It is well-suited for tools that are exposed to impacts and bumps.

STANDARDS (NOTE : PLEASE SEE HOW YOU CAN PRESENT THIS WHETHER YOU WANT TO PRESENT WITH CHEMICAL COMPOSITION OR ANYTHING ELSE)

- Europe : HS 3-3-2

- Germany : 1.3333

Steel Properties

- Machinability: Good - facilitating ease of machining processes.

- Wear Resistance: High - providing durability in demanding conditions.

- Toughness: Moderate - ensuring a balance between strength and resistance to fracture.

- Hot Hardness: Retains hardness at elevated temperatures.

- Grindability: Easy to grind - improving finish and dimensional accuracy.

Specifications

Chemical Composition. (PLEASE EDIT THESE VALUES IN THE DATA-SHEET PROVIDED IN THE PDF..)

| C | Cr | Mo | W | Co | V |
| --- | --- | --- | --- | --- | --- |
| 1.00 | 4.00 | 2.70 | 2.90 | - | 2.40 |

Mechanical Properties:

| Property | Value |
| --- | --- |
| Hardness (HBW) | 255 max (Annealed) |
| Quenching and Tempering Hardness (HRC) | 62 min |

Physical Properties

| Property | Value |
| --- | --- |
| Density (g/cm³) | 8.00 |

Modulus of Elasticity

| Temperature (°C) | 10^3 x (N/mm²) |
| --- | --- |
| 20 | 210 |

Thermal Properties

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 20 | 20 |

HEAT TREATMENT AND PROCESSES

| Process | Details |
| --- | --- |
| Soft Annealing | Heat to 780-820°C, cool slowly in furnace. Maximum Brinell hardness: 255. |
| Stress Relieving | Heat to 600-650°C, hold for 1 hour, followed by air cooling. Reduces distortion during heat treatment. |
| Hardening | Heat to 1170-1220°C, followed by oil or air quenching, or warm bath (550-220°C). |
| Tempering | Temper at 520-550°C, at least twice for at least 62 HRC. |

Applications

- In the metal plating sector

- Metal circular saw blades

- Long saw blades

- Blades for wood machining are manufactured from this steel as a matter of preference

Quality Assurance

Our ABC III 1.3333 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our ABC III 1.3333 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

| ROUNDS |  | SQUARES |  |
| --- | --- | --- | --- |
| SIZE (MM) | CONDITION | SIZE (MM) | CONDITION |
| 6.00 - 14.00 | CG | 7.2, 8.8, 10.5, 11 | HRA |
| 15.00 - 50.00 | HRAP | 13.5, 14, 17.5, 21 | HRA |
| 52.00 - 405.00 | FAT | 27, 32, 40 | HRA |
|  |  | 52.00 - 305.00 | FA |

| FLATS |  |  |  |
| --- | --- | --- | --- |
| THICKNESS (MM) | WIDTH (MM) | CONDITION |  |
| 5.00 - 32.00 | 21.00 - 105.00 | HRA |  |
| 32.00 - 105.00 | 40.00 - 205.00 | FA |  |

Click here to contact our experienced sales team who will assist you with your ABC III 1.3333 tool steel enquiry.

7. T1 Steel Grade:

Grade Brief: (NOTE : -Only keep round, squares and flats UNDER FORM OF SUPPLY IN DATSHEET Rest remove.)

Toolman Special Steels is proud to produce and offer  T1 (1.3355) -  one of the original tungsten high speed steels, although all tungsten steel grades are used to a limited extent because of the cost and questionable availability of tungsten. T1 high speed steel is an air or oil hardening tool steel which has good comprehensive performance. The material exhibits excellent wear resistance and resistance to softening. It also offers good toughness, effective cutting performance, and a strong response to deep hardening.

STANDARDS (NOTE : PLEASE SEE HOW YOU CAN PRESENT THIS WHETHER YOU WANT TO PRESENT WITH CHEMICAL COMPOSITION OR ANYTHING ELSE)

- Europe : HS 18-0-1

- Sweden : SS2750

- Japan : JIS SKH2

- Germany : 1.3355

- USA : AISI T1

Steel Properties

- Tungsten high - speed tool steel

- Very high resistance to wear and to softening

- Good toughness and cutting capability

- Deep hardening response

Specifications

Chemical Composition (PLEASE EDIT THESE VALUES IN THE DATA-SHEET PROVIDED IN THE PDF.. ALSO, REPLACE E- T1 WITH JUST T1 IN DATA-SHEET)

| C | Cr | Mo | W | Co | V |
| --- | --- | --- | --- | --- | --- |
| 0.75 | 4.10 | - | 18.0 | - | 1.10 |

Mechanical Properties:

| Property | Value |
| --- | --- |
| Hardness (HB) | 230 - 300 (Annealed) |
| Quenching and Tempering Hardness (HRC) | 62 - 66 |

Physical Properties

| Property | Value |
| --- | --- |
| Density (g/cm³) | 8.7 |

Modulus of Elasticity

| Temperature (°C) | 10^3 x (N/mm²) |
| --- | --- |
| 20 | 217 |

Thermal Properties

Thermal Expansion Coefficient

| Temperature (°C) | Thermal Expansion Coefficient (10^-6/°C) |
| --- | --- |
| 500 | 11.8 |
| 600 | 12 |

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 20 | 19 |

HEAT TREATMENT AND PROCESSES

| Process | Temperature (°C) | Procedure Details | Cooling Method |
| --- | --- | --- | --- |
| Soft Annealing | 850-900 | Heat to 850 - 900°C | Cool slowly in furnace to about 700°C, then air cool |
| Stress Relieving | 600-700 | Heat to 600-700°C, hold for 2 hours | Cool in still air |
| Hardening | 1st Step: 450-500 | Preheat in 2 steps: 450-500°C, then 850-900°C | Quench in oil, warm bath, or air |
|  | 2nd Step: 850-900 | Heat to 1210-1240°C for high hardness, 1190-1210°C for toughness |  |
| Tempering | 540-620 | Heat to 540-620°C, hold for at least 2 hours per 25 mm thickness, usually triple tempering | Cool in still air |

Applications

- Turning

- Planing and Slotting Tools

- Taps

- Spiral Drills

- Threading Dies

- Profile Cutting Tools

- Broaching tools

- Reamers

Quality Assurance

Our T1 1.3355 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our T1 1.3355 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

| ROUNDS |  | SQUARES |  |
| --- | --- | --- | --- |
| SIZE (MM) | CONDITION | SIZE (MM) | CONDITION |
| 6.00 - 14.00 | CG | 7.2, 8.8, 10.5, 11 | HRA |
| 15.00 - 50.00 | HRAP | 13.5, 14, 17.5, 21 | HRA |
| 52.00 - 405.00 | FAT | 27, 32, 40 | HRA |
|  |  | 52.00 - 305.00 | FA |

| FLATS |  |  |  |
| --- | --- | --- | --- |
| THICKNESS (MM) | WIDTH (MM) | CONDITION |  |
| 5.00 - 32.00 | 21.00 - 105.00 | HRA |  |
| 32.00 - 105.00 | 40.00 - 205.00 | FA |  |

Click here to contact our experienced sales team who will assist you with your T1 1.3355 tool steel enquiry.

8. T4 Steel Grade: (NOTE : - REMOVE THE FOREIGN LANGUAGE - ONLY KEEP ENGLISH ONE IN THE DATA-SHEET AND REPLACE THE COMPANY NAME WITH TOOLMAN)

Grade Brief:

Toolman Special Steels is proud to produce and offer  T4 (1.3255) - AISI T4 tool steel is one of tungsten type high speed tool steel, which belongs to ASTM A600 specification, the standard for high speed tool steel materials. ASTM T4 tool steel is similar to T1 Tool Steel materials, but with 4.25~5.75% cobalt added to increase heat resistance. The red hardness of T4 steel and the high temperature hardness is a little higher than T1 tool steel. AISI T4 tool steel is a deep hardening alloy capable of Rockwell C 64 hardness.

STANDARDS (NOTE : PLEASE SEE HOW YOU CAN PRESENT THIS WHETHER YOU WANT TO PRESENT WITH CHEMICAL COMPOSITION OR ANYTHING ELSE)

- Europe : S 18-1-2-5

- Japan : JIS SKH3

- Germany : 1.3255

- USA : AISI T4

Steel Properties

- High duty High-Speed-Steel on tungsten base.

- Deep hardening response

- Good toughness and cutting capability

Specifications

Chemical Composition (NOTE : - PLEASE EDIT THESE VALUES IN THE DATA-SHEET PROVIDED IN THE PDF.. ALSO ONLY KEEP THE ENGLISH LANGUAGE - REMOVE THE FOREIGN LANGUAGE IN THE DATA-SHEET)

| C | Cr | Mo | W | Co | V |
| --- | --- | --- | --- | --- | --- |
| 0.81 | 4.30 | 0.65 | 18.0 | 4.80 | 1.50 |

Mechanical Properties:

| Property | Value |
| --- | --- |
| Hardness (HB) | 265 max (Annealed) |
| Quenching and Tempering Hardness (HRC) | 64 - 65 |
| Poisson’s ratio | 0.27 - 0.30 |

Physical Properties

| Property | Value |
| --- | --- |
| Density (g/cm³) | 8.7 |

Modulus of Elasticity

| Temperature (°C) | Gpa |
| --- | --- |
| 20 | 217 |

Thermal Properties

Thermal Expansion Coefficient

| Temperature (°C) | Thermal Expansion Coefficient (10^-6/°C) |
| --- | --- |
| 500 | 11.3 |
| 600 | 11.4 |

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 20 | 19 |

HEAT TREATMENT AND PROCESSES

| Process | Temperature Range (°C) | Details |
| --- | --- | --- |
| Soft Annealing | Heat to 820-850°C, slow cool to 550°C, then air cool | Maximum Brinell hardness of 265 |
| Stress Relieving | Heat to 600-650°C, hold for 1 hour, then air cool | Removes machining stresses to reduce distortion during heat treatment |
| Hardening | Heat to 1260-1290°C, quench in oil, air, or warm bath at 550°C | Hardness after quenching: 63-66 HRC |
| Tempering | 2x at 560-580°C | Hardness after tempering: 64-65 HRC |

| Tempering °C after quenching | 100 | 200 | 250 | 300 | 400 | 500 | 550 | 600 | 650 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| HRC | 65 | 63 | 62 | 61.5 | 62.5 | 65 | 65.5 | 63 | 55 |

Applications

- Cutting tools

- Broaches and Cold extrusion punches

- Turning

- Planing and Milling cutters for roughing work

- Grey cast iron

- Chill castings NF metals & non-metal material

Quality Assurance

Our T4 1.3255 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our T4 1.3255 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

| ROUNDS |  | SQUARES |  |
| --- | --- | --- | --- |
| SIZE (MM) | CONDITION | SIZE (MM) | CONDITION |
| 6.00 - 14.00 | CG | 7.2, 8.8, 10.5, 11 | HRA |
| 15.00 - 50.00 | HRAP | 13.5, 14, 17.5, 21 | HRA |
| 52.00 - 405.00 | FAT | 27, 32, 40 | HRA |
|  |  | 52.00 - 305.00 | FA |

| FLATS |  |  |  |
| --- | --- | --- | --- |
| THICKNESS (MM) | WIDTH (MM) | CONDITION |  |
| 5.00 - 32.00 | 21.00 - 105.00 | HRA |  |
| 32.00 - 105.00 | 40.00 - 205.00 | FA |  |

Click here to contact our experienced sales team who will assist you with your T4 1.3255 tool steel enquiry.

9. T15 Steel Grade:

Grade Brief: (Only KEEP MODE OF SUPPLY IN DATA-SHEET ROUNDS, FLATS, SQUARES. REST REMOVE)

Toolman Special Steels is proud to produce and offer  T15 (1.3202) - a high tungsten alloy grade for high performance cutting tools. T15 steel high vanadium content enhances its cutting performance and durability, while its cobalt content contributes to superior tempering durability and hot hardness. This steel has demonstrated significant advantages in applications involving hard materials that cause extensive wear on cutting surfaces, especially under elevated temperatures.

STANDARDS (NOTE : PLEASE SEE HOW YOU CAN PRESENT THIS WHETHER YOU WANT TO PRESENT WITH CHEMICAL COMPOSITION OR ANYTHING ELSE)

- Europe : HS 12-0-5-5

- Germany : 1.3202

- USA : AISI T15

Steel Properties

- High Toughness & Ductility

- High Wear Resistance

- Very high Compressive strength

- Very high Edge Stability

- High Grindability

- Very high Hot Hardness

Specifications

Chemical Composition (NOTE : - PLEASE EDIT THESE VALUES IN THE DATA-SHEET PROVIDED IN THE PDF.. ALSO, REPLACE E- T15 WITH JUST T15 IN DATA-SHEET)

| C | Cr | Mo | W | Co | V |
| --- | --- | --- | --- | --- | --- |
| 1.50 | 5.00 | - | 12.5 | 5.00 | 5.00 |

Mechanical Properties:

| Property | Value |
| --- | --- |
| Hardness (HB) | 300 max (Annealed) |
| Quenching and Tempering Hardness (HRC) | 65 - 69 |

Physical Properties

| Property | Value |
| --- | --- |
| Density (g/cm³) | 8.2 |

Modulus of Elasticity

| Temperature (°C) | (kN/mm²) |
| --- | --- |
| 20 | 245 |

Thermal Properties

Thermal Expansion Coefficient

| Temperature (°C) | Thermal Expansion Coefficient (10^-6/°C) |
| --- | --- |
| 500 | 11.64 |
| 600 | 12.08 |

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 20 | 24 |

HEAT TREATMENT AND PROCESSES

| Process | Temperature (°C) | Procedure Details | Cooling Method |
| --- | --- | --- | --- |
| Soft Annealing | 850-900 | Heat to 850 - 900°C | Cool slowly at 10°C/h to about 700°C, then air cool |
| Stress Relieving | 600-700 | Heat to 600-700°C, hold for 2 hours | Cool in still air. Slow cooling down to 500°C |
| Hardening | 1st Step: 450-500 | Preheat in 2 steps: 450-500°C, then 850-900°C | Quench in oil, warm bath, or air |
|  | 2nd Step: 850-900 | Heat to 1210-1240°C for high hardness, 1190-1210°C for toughness |  |
| Tempering | 560- 580 | Tempering at 560°C three times for at least 1 hour each time | Cooling to room temperature (25°C) between temperings. |

Applications

- Automotive Racing

- Broaches and Reamers

- Cold Forming / Coining

- End Mills

- Fine Blanking, Stamping, Blanking

- Gear Cutting, Shaving and Shaping Tools

- Powder Pressing

- Rolling

- Shearing / Machine Knives

- Special Cutting Tools

- Twist Drills and Taps

- Pill punching dies

Quality Assurance

Our T15 1.3202 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our T15 1.3202 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

| ROUNDS |  | SQUARES |  |
| --- | --- | --- | --- |
| SIZE (MM) | CONDITION | SIZE (MM) | CONDITION |
| 6.00 - 14.00 | CG | 7.2, 8.8, 10.5, 11 | HRA |
| 15.00 - 50.00 | HRAP | 13.5, 14, 17.5, 21 | HRA |
| 52.00 - 405.00 | FAT | 27, 32, 40 | HRA |
|  |  | 52.00 - 305.00 | FA |

| FLATS |  |  |  |
| --- | --- | --- | --- |
| THICKNESS (MM) | WIDTH (MM) | CONDITION |  |
| 5.00 - 32.00 | 21.00 - 105.00 | HRA |  |
| 32.00 - 105.00 | 40.00 - 205.00 | FA |  |

Click here to contact our experienced sales team who will assist you with your T15 1.3202 tool steel enquiry.

9. T42 Steel Grade:

Grade Brief:

Toolman Special Steels is proud to produce and offer  T42 (1.3207) - a proprietary tungsten high speed steel containing 10 percent cobalt. T42 is harder than most high-speed steels and has in addition a reasonably good toughness. T42 is used mainly for tools requiring maximum abrasion resistance and medium toughness.

STANDARDS (NOTE : PLEASE SEE HOW YOU CAN PRESENT THIS WHETHER YOU WANT TO PRESENT WITH CHEMICAL COMPOSITION OR ANYTHING ELSE)

- Europe : HS 10-4-3-10

- Sweden : SS2736

- Japan : JIS SKH57

- Germany : 1.3207

- USA : AISI T42

Steel Properties

- High Toughness & Ductility

- High Wear Resistance

- Good Compressive strength

- High Edge Stability

- Hot Hardness (red hardness)

Specifications

Chemical Composition (NOTE : - PLEASE EDIT THESE VALUES IN THE DATA-SHEET PROVIDED IN THE PDF..

| C | Cr | Mo | W | Co | V |
| --- | --- | --- | --- | --- | --- |
| 1.26 | 4.00 | 3.60 | 9.30 | 10.00 | 3.20 |

Mechanical Properties:

| Property | Value |
| --- | --- |
| Hardness (HB) | 300 max (Annealed) |
| Quenching and Tempering Hardness (HRC) | 64 - 67 |

Physical Properties

| Property | Value |
| --- | --- |
| Density (g/cm³) | 8.23 |

Modulus of Elasticity

| Temperature (°C) | 10^3 x (N/mm²) |
| --- | --- |
| 20 | 217 |

Thermal Properties

Thermal Expansion Coefficient

| Temperature (°C) | Thermal Expansion Coefficient (10^-6/°C) |
| --- | --- |
| 500 | 10.5 |
| 600 | 10.7 |

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 20 | 19 |

HEAT TREATMENT AND PROCESSES

| Process | Temperature Range | Details |
| --- | --- | --- |
| Soft Annealing | 800-860°C | Heat to 800-860°C, cool slowly in furnace. Maximum Brinell hardness of 300. |
| Stress Relieving | 600-650°C | Heat to 600-650°C, hold for 1 hour, air cool. Reduces machining stresses to prevent distortion. |
| Hardening | 1200-1230°C | Harden from 1200-1230°C followed by quenching in oil, air, or a warm bath at 540°C. Hardness after quenching: 64-66 HRC. |
| Tempering | 540-570°C | Temper at 540-570°C at least twice for 65-67 HRC. Hardness after tempering: 64-67 HRC. |

| Tempering °C after quenching | 100 | 200 | 300 | 400 | 500 | 550 | 600 | 650 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| HRC | 65 | 64.5 | 64 | 64.5 | 67 | 66.5 | 63 | 57 |

Applications

- End Mills

- Fine Blanking, Stamping, Blanking

- Gear Cutting, Shaving and Shaping Tools

- Special Cutting Tools

- Blades for Sawing Machines

- Broaches and Reamers

- All kinds of profile blades for wood machining are manufactured from sheets.

- For severely stressed tools for fine and roughing work

- Wood working tools and tools for cold work.

Quality Assurance

Our T42 1.3207 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our T42 1.3207 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

| ROUNDS |  | SQUARES |  |
| --- | --- | --- | --- |
| SIZE (MM) | CONDITION | SIZE (MM) | CONDITION |
| 6.00 - 14.00 | CG | 7.2, 8.8, 10.5, 11 | HRA |
| 15.00 - 50.00 | HRAP | 13.5, 14, 17.5, 21 | HRA |
| 52.00 - 405.00 | FAT | 27, 32, 40 | HRA |
|  |  | 52.00 - 305.00 | FA |

| FLATS |  |  |  |
| --- | --- | --- | --- |
| THICKNESS (MM) | WIDTH (MM) | CONDITION |  |
| 5.00 - 32.00 | 21.00 - 105.00 | HRA |  |
| 32.00 - 105.00 | 40.00 - 205.00 | FA |  |

Click here to contact our experienced sales team who will assist you with your T42 1.3207 tool steel enquiry.