PRODUCT DETAILS AND CATEGORIES FOR WEBSITE

Notes :

- The composition of the grades present in this PDF is accurate. The data sheets provided to you as a separate attachment - kindly edit the values of the composition there as per this sheet.

- This is the required content. Kindly present according to the website colour scheme. Wherever necessary, provide the details in tabular form such as chemical composition, size ranges etc (in whatever way it looks good).

HOT WORK STEELS

1. H13 Steel Grade - Product Details

Grade Brief

Toolman Special Steels is proud to produce and offer H13 steel, a versatile and widely used chromium-molybdenum hot work steel. Known for its exceptional combination of high toughness and resistance to thermal fatigue, our H13 steel meets the highest industry standards for quality and performance. It will give an extra margin of safety in tools subject to hammer blows and those tools containing deep recesses and sharp corners. While H13 is designed primarily as a hot work tool steel, it has solved many cold work applications where extra toughness was required at the sacrifice of some wear resistance.  Below, you'll find comprehensive details about our H13 steel, its applications, and its technical specifications.

H13 Steel Properties

- Thermal Stability: Retains mechanical properties at elevated temperatures.

- Toughness: High resistance to cracking and impact, enhancing tool life.

- Versatility: Suitable for various hot work applications, providing flexibility in manufacturing processes.

- Wear Resistance: Prolongs the lifespan of tools and dies, reducing downtime and maintenance costs.

- Machinability: Offers good machinability in the annealed condition, facilitating easier fabrication.

SPECIFICATIONS

Chemical Composition (NOTE - AS PER GMTC WEBSITE)

| Chemical Composition, % |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Standard | AISI (UNS) | C | Si | Mn | P, ≤ | S, ≤ | Cr | Mo | V |
| ASTM A681 | H13 (T20813) | 0.32-0.45 | 0.80-1.25 | 0.20-0.60 | 0.030 | 0.030 | 4.75-5.50 | 1.10-1.75 | 0.80-1.20 |

Mechanical Properties

| ITEMS |  |
| --- | --- |
| Hardness (HBW) | 235 MAX (ANNEALED) |
| Hardness After Quenching (hardenability) (HRC) | 52 MIN. (ANNEALED) |
| Tensile Strength (MPa) | 1,450 - 1,950 |
| Yield Strength (MPa) | 1,200 - 1,550 |
| Elongation at Break | 10-15 % |
| Impact Toughness (J at 20°C) | 20 - 30 |

| Physical Properties | Value |
| --- | --- |
| Density (g/cm³) | 7.80 |
| Modulus of Elasticity (GPa) | 215 |

Thermal Expansion Coefficient

Temperature (℃)                                  10^-6/℃

300.                                             12.2

400                                              12.5

500                                              12.9

600                                                13

Thermal Conductivity

Temperature (℃)                                               W/m·K

20                                                                  25

500                                                               28.3

600                                                                29.3

HEAT TREATMENT AND PROCESSES

SOFT ANNEALING Protect the steel and heat through to 750 - 800°C. Then cool in the furnace at 10 - 20°C per hour to 600°C, then freely in air.

STRESS RELIEVING After rough machining, the tool should be heated through to 650°C, holding time 2 hours. Cool slowly to 500°C, then freely in air.

HARDENING Preheating temperature: 600 - 850°C, normally in two preheating steps.

Austenitising temperature: 1020 - 1050°C, normally 1020 - 1030°C.

Protect the tool against decarburisation and oxidation during hardening.

QUENCHING MEDIA

High-speed gas/circulating atmosphere

High-speed gas with sufficient positive pressure quenching in vacuum furnace. Interrupted quench is recommended for distortion control, or when quench cracking is a concern.

Martempering bath or fluidised bed at 450 - 550°C, then cool in air

Martempering bath or fluidised bed at approx. 180 - 220°C then cool in air

Warm oil

TEMPERING

Choose the tempering temperature according to the hardness required by reference to the tempering graph. Temper at least twice with intermediate cooling to room temperature.

| Tempering °C | 100 | 210 | 300 | 400 | 500 | 550 | 600 | 650 | 700 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| HRC | 54 | 53 | 53 | 55 | 56 | 54 | 51 | 43 | 34 |

Applications of H13 Steel

- Die Casting Dies: Ideal for dies requiring high toughness and resistance to thermal fatigue.

- Extrusion Tools: Used in hot extrusion processes due to its ability to withstand high temperatures and pressures.

- Hot Forging Dies: Suitable for forging applications where high strength and resistance to impact are critical.

- Plastic Molding: Commonly used for molds in the plastic industry, especially for producing high-quality and durable molds.

- Punches and Dies: Employed in the manufacture of tools for cutting and shaping metals, benefiting from its wear resistance.

- Shear Blades: Utilized in the production of blades that cut through metals, maintaining sharpness and integrity over extended use.

- Bulldozer dies

- Ejectors and nozzles for pressure die casting of zinc, lead and tin base alloys.

- Used for ejector pins, tool holders and shrink fit chucks.

- Hot cropping, billet shearing and circular shearing

- Metal Track Pressure Tools

- Inserts,

- Plungers

H13 ESR

H13 ESR is the most refined material with the traditional VD route. The quality of material increase the toughness, highly increase the micro- cleanness level.

Highly recommend the use of AISI-H13 ESR grade for Aluminium Pressure Die Casting & other component subjected to high working temperatures and high pressure strength.

H13 is fully ultrasonic inspected with 100% positive results as per NDT standards.

Quality Assurance

Our H13 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request.

MANUFACTURING RANGE

Products                             Diameter (mm)

Hot Rolled bar                       8 - 65

Forged and Turned bars         65.2 - 500

Forged Square Bars              50 - 500

FLATS

THICKNESS                     WIDTH

6.00 mm - 410.00 mm       20.00 mm  - 700.00 mm

Click here to contact our experienced sales team who will assist you with your H13 tool steel enquiry.

Contact Us

For more information or to place an order, please contact our sales team at:

Phone: 
Email: 
Address: 
Office Hours:

2. H11 Steel Grade:

Grade Brief

Toolman Special Steels is proud to produce and offer H11 steel, a versatile hot work tool steel known for its excellent toughness, high-temperature strength, and resistance to heat and fatigue. It is widely used in industries requiring high wear resistance and the ability to maintain hardness at elevated temperatures. Its uniform spheroidizing microstructure and great cleanliness make it a top choice for demanding applications. No matter your industry, whether it's automotive, aerospace, or general engineering, H11 steel offers exceptional performance and reliability, making it an excellent choice for your toughest applications.

STEEL PROPERTIES

Hot work tool steel.

Deep hardening response.

High hot tensile strength.

Good combination of toughness, hardness and wear resistance.

Good thermal conductivity and resistance to softening and to cracking.

SPECIFICATIONS

Chemical Composition (wt. %): (In tabular form needed)

- Carbon (C): 0.33-0.43

- Silicon (Si): 0.8-1.25

- Manganese (Mn): 0.2-0.6

- Chromium (Cr): 4.75-5.5

- Molybdenum (Mo): 1.1-1.6

- Vanadium (V): 0.3-0.6

- Phosphorus (P) & Sulfur (S): ≤0.03

- Nickel (Ni) + Copper (Cu): ≤0.75

Mechanical Properties

| Property | Value |
| --- | --- |
| Annealed Hardness | Max. 235 HBW |
| Hardness After Quenching | Min. 53 HRC |

| Tensile strength | 1792 MPa |
| --- | --- |
| Yield Strength | 1482 MPa |
| Elongation | 8% |
| Impact Toughness | 13.6-33.9 J/cm2 |

Physical Properties

| Density | 7.8 g/cm³ |
| --- | --- |

Modulus of Elasticity

| Condition | Value |
| --- | --- |
| At 500°C | 190-210 GPa |
| At 600°C | 165 GPa |

Thermal Properties

Thermal Expansion  Coefficient

Temperature (℃)                                                   10^-6/℃

500                                                                      12.9

600                                                                         13

Thermal Conductivity

Temperature (℃)                                                       W/m·K

500                                                               28.3

600                                                               29.3

Heat Treatment and Processes

Heat treatment for H11 steel typically involves a combination of heating, soaking, quenching, and tempering processes to achieve desired mechanical properties. The following provides general heat treatment guidelines

1. Preheating : Preheat the H11 steel component slowly and uniformly to the desired austenitizing temperature. This helps to reduce the risk of cracking during subsequent heating.

2. Austenitizing: Heat the preheated H11 steel to the austenitizing temperature range of approximately 1010-1095°C (1850-2000°F), depending on the specific requirements and the desired properties. Hold the steel at this temperature for sufficient time to ensure complete transformation to austenite.

3. Quenching: Quench the austenitized H11 steel rapidly in a suitable quenching medium. Common quenching media for H11 steel include oil, air, and specialized quenching baths. Quenching rates and media selection should be chosen carefully to achieve the desired hardness and minimize distortion or cracking.

4. Tempering: After quenching, immediately temper the hardened H11 steel to relieve internal stresses and achieve the desired balance of hardness and toughness. Temperatures typically range from 540-650°C (1000-1200°F), depending on the specific application requirements. Hold the steel at the tempering temperature for the recommended duration, often a minimum of two hours, and allow it to cool in still air.

5. Multiple Tempering Cycles : Depending on the application and desired properties, multiple tempering cycles may be necessary. This process involves reheating the tempered steel to the tempering temperature and holding it for a specified time before cooling again.

6. Stress Relief Annealing: If necessary, stress relief annealing can be performed at temperatures ranging from 600-650°C (1110-1200°F) for a minimum of four hours to reduce internal stresses and improve dimensional stability.

7. Controlled Cooling: Throughout the heat treatment process, maintain control over the cooling rate to minimize the risk of distortion, cracking, or excessive residual stresses in the H11 steel component.

8. Post-Heat Treatment Inspection: After heat treatment, conduct thorough inspections of the H11 steel component to ensure that the desired mechanical properties, such as hardness, toughness, and dimensional accuracy, have been achieved.

It's important to note that specific heat treatment parameters may vary depending on factors such as the size and shape of the H11 steel component, the desired mechanical properties, and the equipment available.

Heat treatment :  (need in tabular form)

Temperature            Duration                        Cooling

Soft annealing                  800 - 860 °C             2 - 5 h                            furnace

Stress-relief annealing     600 - 650 °C             min. 4 h                           furnace

Hardening                      1020 - 1060 °C         Group II                    oil, air, WB 500 °C

Tempering                       530 - 700 °C             min. 2 h                          still air                                                                                                              depending on cross section

| Tempering °C | 100 | 200 | 300 | 400 | 500 | 550 | 600 | 650 | 700 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| HRC | 52 | 52 | 52 | 52 | 54 | 53 | 48 | 37 | 31 |

Applications:

H11 steel is widely used in various demanding applications across different industries, thanks to its exceptional properties. Some common applications include:

- Die Casting: H11 is suitable for die casting dies for aluminum, magnesium, and zinc alloys due to its high hot strength, thermal fatigue resistance, and good thermal conductivity.

- Forging: In the forging industry, H11 finds application in forging dies and tools where high toughness and resistance to thermal fatigue are required.

- Extrusion: The steel is utilized in extrusion dies for aluminum and brass alloys, providing good thermal conductivity and resistance to thermal cracking.

- Plastic Molding: H11 steel is employed in injection mold tooling and extrusion dies in plastic molding applications due to its high hot hardness and resistance to thermal fatigue.

- High-Temperature Applications: H11 performs well in high-temperature applications such as hot punches, hot shear blades, and trimming dies due to its high temperature strength and thermal stability.

- bridge kind tools, liner holders, extrusion tooling, Hot work punches, Hot gripper dies, Aircraft landing gear and shrink work chucks, Tools for hot forging of light metal,Pressure die casting tools. Dies, mandrels, punchers, knives, moulds.

Quality Assurance

Our H11 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our H11 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

Products                             Diameter (mm)

Hot Rolled bar                       8 - 65

Forged and Turned bars         65.2 - 500

Forged Square Bars              50 - 500

FLATS

THICKNESS                     WIDTH

6.00 mm - 410.00 mm       20.00 mm  - 700.00 mm

Click here to contact our experienced sales team who will assist you with your H11 tool steel enquiry.

3. H12 Steel Grade:

Grade Brief

Toolman Special Steels is proud to produce and offer H12 steel. H12 hot work tool steel is a 5% chromium, general-purpose hot work steel that is characterized by excellent impact toughness. It contains less vanadium than the widely-used H13 hot work tool steel. Steel is a deep-hardening, air-hardening steel that exhibits minimal size change during heat treatment. It has good resistance to thermal fatigue cracking (heat cracking) and excellent resistance to gross cracking and thermal shock when water cooled in service.  The addition of tungsten enhances its wear resistance while maintaining strength and toughness.

Steel Properties

˙High wear resistance

˙Good high temperature strength

Extra- fine- structure without grain-boundary carbide.

˙Uniform spheroidizing microstructure

˙Great cleanliness

SPECIFICATIONS

| Element | Min (%) | Max (%) |
| --- | --- | --- |
| C | 0.30 | 0.40 |
| Si | 0.80 | 1.25 |
| Mn | 0.20 | 0.60 |
| P | - | 0.03 |
| S | - | 0.03 |
| Cr | 4.75 | 5.50 |
| Mo | 1.25 | 1.75 |
| V | 0.20 | 0.50 |
| W | 1.00 | 1.70 |
| Ni+Cu | - | 0.75 |

Chemical Composition

Mechanical Properties

Annealed Condition

| Property | Value |
| --- | --- |
| Hardness (HBW) | 235 max. |
| Hardness After Quenching (HRC) | 53 min. |

Physical Properties

Density

| Property | Value |
| --- | --- |
| Density | 7.81 g/cm³ |

Modulus of Elasticity

| Temperature (°C) | Modulus of Elasticity (GPa) |
| --- | --- |
| 500 | 176 |
| 600 | 166 |

Thermal Properties

Thermal Expansion Coefficient

| Temperature (°C) | Thermal Expansion Coefficient (10^-6/°C) |
| --- | --- |
| 500 | 12.9 |
| 600 | 13.0 |

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 500 | 28.3 |
| 600 | 29.3 |

Heat Treatment and Processes

| Soft annealing °C | Cooling | Hardness HB |
| --- | --- | --- |
| 820 | Furnace | max. 235 |

| Hardening °C | Quenching | Hardness after quenching HRC |
| --- | --- | --- |
| 1030 – 1130 | Oil or hot bath, 500 – 550 °C | 53 min |

| Tempering °C after Quenching | 100 | 200 | 300 | 400 | 500 | 600 | 700 | 800 | 900 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| HRC | 55 | 54 | 54.3 | 54.8 | 53 | 51 | 48 | 41 | 34 |

Applications

H12 hot work steel is recommended for hot tooling applications where maximum resistance to cracking is required. Such applications include hot punches, die casting dies, forgings dies, Injection Moulding, hot shear blades, and extrusion tooling

Quality Assurance

Our H12 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our H12 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

Products                             Diameter (mm)

Hot Rolled bar                       8 - 65

Forged and Turned bars        65.2 - 500

Forged Square Bars              50 - 500

FLATS

THICKNESS                     WIDTH

6.00 mm - 410.00 mm       20.00 mm  - 700.00 mm

Click here to contact our experienced sales team who will assist you with your H12 tool steel enquiry.

4.  H10 Steel Grade:

Grade Brief

H10 steel (1.2365) is a hot work tool steel known for its excellent toughness, resistance to thermal fatigue, and ability to withstand high temperatures. Hot work, chromium-molybdenum type tool steel that exhibits excellent resistance to softening at elevated tempertaure. In addition to its superior anti-tempering softening resistance, this premium hot work tool steel produced by Toolman has outstanding thermal fatigue resistance and can be water cooled during the use.. It is commonly used in applications requiring significant impact and heat resistance, making it ideal for hot forging, extrusion, and die-casting applications.

Steel Properties

- High toughness

- ˙Extreme high temperature strength

- ˙High temperature creep resistance

- ˙High temperature softening resistance

- ˙Fine crystallisation

- ˙Uniform spheroidizing microstructure

- ˙Good cleanliness

- Tungsten-free special hot work tool steel on a CrMoV base with good toughness. Insensitive to thermal shock, and thus not susceptible to heat cracking. Particularly suitable for water cooling.

Specifications

Chemical Composition

| Element | Min (%) | Max (%) |
| --- | --- | --- |
| C | 0.28 | 0.35 |
| Si | 0.10 | 0.40 |
| Mn | 0.15 | 0.45 |
| P | - | 0.030 |
| S | - | 0.030 |
| Cr | 2.70 | 3.20 |
| Mo | 2.60 | 3.00 |
| V | 0.40 | 0.70 |

Mechanical Properties:

| Property | Value |
| --- | --- |
| Hardness (HBW) | 229 max (Annealed) |
| Hardness After Quenching (hardenability) (HRC) | 47 min (Annealed) |
| Yield Strength | 1000 MPa |
| Tensile Strength | 1200 MPa |
| Elongation | 10% |
| Impact Toughness | 25 J (at room temperature) |

Physical Properties

| Property | Value |
| --- | --- |
| Density (g/cm³) | 7.85 |

Modulus of Elasticity

| Temperature (°C) | GPa |
| --- | --- |
| 500 | 176 |
| 600 | 165 |

Thermal Properties

Thermal Expansion Coefficient

| Temperature (°C) | Thermal Expansion Coefficient (10^-6/°C) |
| --- | --- |
| 500 | 13.2 |
| 600 | 13.4 |

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 500 | 30.1 |
| 600 | 29.7 |

HEAT TREATMENT

| Heat Treatment | Temperature | Duration | Cooling |
| --- | --- | --- | --- |
| Stress Relieving | Approx. 650 °C (annealed) <br> Approx. 550 °C (hardened & tempered) | 1 hour per 50 mm wall thickness | Furnace |
| Soft Annealing | 800 °C | 1 hour per 25 mm wall thickness | Furnace |
| Hardening | 1040 °C | 30 seconds per mm wall thickness | Max. 52 HRC in oil, hot bath, protective atmosphere, vacuum, or air |
| Tempering | See tempering curve | 1 hour per 25 mm wall thickness | Air |
| Working Hardness | 30–48 HRC pre-heating of the tools = 250–350 °C | - | - |

| Tempering °C after Quenching | 100 | 200 | 300 | 400 | 500 | 550 | 600 | 650 | 700 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| HRC | 51 | 50.5 | 50 | 50 | 53 | 51 | 48 | 41 | 29 |

Applications

- Dies

- Tools for the production of screws & forging machines

- highly stressed extruding tools for light metal processing - mandrels, pressing die cast moulds.

- Extruder tools including pipe extruders, such as extrusion stems, liners and die holders.

- Part stamping dies for non-ferrous heavy metals, forging die and press die inserts, forging tools for Hatebur presses.

- Die-casting moulds for non-ferrous heavy metal pressure die-casting.

- Hot Shearing Blades

Quality Assurance

Our  H10 1.2365 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our H10 - 1.2365 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

Products                             Diameter (mm)

Hot Rolled bar                       8 - 65

Forged and Turned bars        65.2 - 500

Forged Square Bars              50 - 500

FLATS

THICKNESS                     WIDTH

6.00 mm - 410.00 mm       20.00 mm  - 700.00 mm

Click here to contact our experienced sales team who will assist you with your H10 tool steel enquiry.

5. DB6 Steel Grade:

Grade Brief

DB6, also known as DIN 1.2714, is a hot work tool steel with excellent toughness, wear resistance, and high hardness. It is particularly well-suited for applications involving high temperatures and mechanical stress, such as forging dies, extrusion dies, and die casting. This nickel hot work tool steel produced by Toolman has good hardenability, wear resistance, thermal fatigue resistance, and thermal stress resistance, good strength at high temperatures, and good tempering resistance.

Specifications

| Element | Composition (%) |
| --- | --- |
| Carbon (C) | 0.50-0.60 |
| Silicon (Si) | 0.10-0.40 |
| Manganese (Mn) | 0.65-0.95 |
| Phosphorus (P) | - ≤0.03 |
| Sulphur (S) | - ≤0.03 |
| Chromium (Cr) | 1.00-1.20 |
| Molybdenum (Mo) | 0.45-0.55 |
| Vanadium (V) | 0.07-0.12 |
| Nickel (Ni) | 1.60-1.80 |

Steel Properties

Good hardenability.

Uniform hardness over sections also at big dimensions.

Resistance under impact loadings.

Good strength and toughness

Good tempering resistance and dimensional stability.

Tools can be water or air cooled.

Mechanical Properties:

| Property | Value |
| --- | --- |
| Hardness (HBW) | 248 max (Annealed) |
| Hardness After Quenching (hardenability) (HRC) | 44 min (Annealed) |
| Tensile Strength | 1000-1400 MPa |
| Yield Strength | 1045 MPa |
| Elongation | 15-20% |
| Impact Toughness | 20-25 J/cm² |

Physical Properties

| Density | 7.8 g/cm³ |
| --- | --- |

Modulus of Elasticity

| Condition | Value |
| --- | --- |
| At 500°C | 176 GPa |
| At 600°C | 165 GPa |

Thermal Properties

Thermal Expansion Coefficient

| Temperature (°C) | Thermal Expansion Coefficient (10^-6/°C) |
| --- | --- |
| 500 | 14 |
| 600 | 14.3 |

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 500 | 36.8 |
| 600 | 36 |

HEAT TREATMENT AND PROCESSES

| Heat Treatment Process | Temperature (°C) | Duration | Cooling | Additional Details |
| --- | --- | --- | --- | --- |
| Stress Relieving | Approx. 650 | 1 hour per 50 mm wall thickness | Furnace |  |
| Soft Annealing | 700 | 1 hour per 25 mm wall thickness | Furnace |  |
| Hardening | 880 | 1 minute per mm wall thickness | Water/Oil, Protective atmosphere/Oil, Oil, Hot bath, or Vacuum | Quenching hardness Max. 58 HRC |
| Tempering | See tempering curve | 1 hour per 25 mm wall thickness | Air | Working hardness 300–440 HB depending on application |

Applications

1. Forging tools, press and extrusion dies, tools for hot pressing and forging of steels and other metals. Moulds, mandrels, embossing tools, tool holders

2.  DB6 has super toughness  often needed for tools such as : -

- Hobs                                                     Blanking or forming dies

- Collets                                                  Thread Roller Dies

- Punches                                                Embossing Dies

- Forming Rolls

3. Use it where hardening accuracy or cracking hazards make an oil hardening steel necessary such as : -

- Shear Blades                                 Swagging dies

- Punches                                         Slitting Shears

- Stamps                                           Slitting Cutters

4. For machine parts requiring great strength and toughness combined with with hardness and wear resistance it has been used for parts such as : -

- Clutch Parts                                  Spindles

- Pawls                                            Fingers

- Stops                                             Indexing Pins

- Knuckle Pins                                Clutch Pins

Quality Assurance

Our DB6 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our DB6 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

Products                             Diameter (mm)

Hot Rolled bar                       8 - 65

Forged and Turned bars        65.2 - 500

Forged Square Bars              50 - 500

FLATS

THICKNESS                     WIDTH

6.00 mm - 410.00 mm       20.00 mm  - 700.00 mm

Click here to contact our experienced sales team who will assist you with your DB6 tool steel enquiry.

6. H21 Steel Grade:

Grade Brief

H21 Steel is a hot work tool steel for oil or air solidifying to grow high hot quality, maintenance of hardness, and warmth checking resistance. These steels have similar characteristics to that of high-speed steels. The primary alloying elements in tungsten hot-work steels include tungsten, chromium, carbon, and vanadium. This alloy produced by Toolman is one of the hot work, tungsten containing tool steels. The tungsten content is beneficial for hot strength at red heat, although toughness is somewhat reduced. This is mostly utilised as hot work devices, instruments for manufacture of hollows, screws, rivets, nuts and bolts. Die casting tools, forming dies, die inserts, hot shear blades.

Specifications

Chemical Composition (Typical Analysis in %)

| Element | C | Si | Mn | P | S | Cr | W | V |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| % | 0.26-0.36 | 0.15-0.40 | 0.15-0.40 | 0.030 max | 0.030 max | 3.00-3.75 | 8.50-10.00 | 0.30-0.60 |

Steel Properties

- Tungsten containing hot work tool steel beneficial for hot strength at red heat, although toughness is somewhat reduced.

- High resistance to the hot tempering and good toughness.

- Very high firmness during the heat and resistance to the tempering

Mechanical Properties

| Property | Metric |
| --- | --- |
| Hardness | 40.0 – 55.0 HRC |
| Bulk modulus | 140 GPa |
| Poisson’s ratio | 0.27-0.30 |
| Elastic modulus | 190-210 GPa |

Physical Properties

| Property | Value |
| --- | --- |
| Density | 7.80 g/cm³ |
| Thermal Conductivity | 27.0 W/m·K |
| Electric Resistivity | 0.52 Ohm·mm²/m |
| Specific Heat Capacity | 0.46 J/g·K |

Modulus of Elasticity

| Property | Value |
| --- | --- |
| Modulus of Elasticity | 190-210 GPa |

Coefficient of Linear Thermal Expansion

| Temperature Range (°C) | Expansion Coefficient (10⁻⁶ /°C) |
| --- | --- |
| 20-100 | 11.5 |
| 20-200 | 12.0 |
| 20-300 | 12.2 |
| 20-400 | 12.5 |
| 20-500 | 12.9 |
| 20-600 | 13.0 |
| 20-700 | 13.5 |

Mechanical Properties

| Property | Value |
| --- | --- |
| Hardness (Annealed) | Max 240 HB |
| Hardness (Quenched) | 47-53 HRC |

HEAT TREATMENT AND PROCESSES

| Soft annealing °C | Cooling | Hardness HB |
| --- | --- | --- |
| 780 – 810 | Slowly | max. 240 |

| Hardening °C | Quenching | Hardness after quenching HRC |
| --- | --- | --- |
| 1000 – 1130 | Oil or hot bath, 600 – 650 °C | 47 -53 |

| Tempering °C after Quenching | 400 | 500 | 550 | 600 | 650 | 700 |
| --- | --- | --- | --- | --- | --- | --- |
| HRC | 49 | 49 | 51 | 50 | 46 | 36 |

Applications

- Hot working dies and tooling

- Die casting

- Extrusion

- Hot forming of parts

- Moulds for copper and copper alloys

Quality Assurance

Our H21 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our H21 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

Products                             Diameter (mm)

Hot Rolled bar                       8 - 65

Forged and Turned bars        65.2 - 500

Forged Square Bars              50 - 500

FLATS

THICKNESS                     WIDTH

6.00 mm - 410.00 mm       20.00 mm  - 700.00 mm

Click here to contact our experienced sales team who will assist you with your H21 tool steel enquiry.

7. 1.2367 Steel Grade:

Grade Brief

Toolman Special Steels is proud to produce and offer 1.2367 steel, also known as X38CrMoV5-3, is a high-performance hot work tool steel with excellent toughness and resistance to thermal fatigue. It is widely used for hot work applications where high mechanical strength and wear resistance are essential. It has been refined via ESR process to ensure highest quality standards in terms of grain size, segregation, micro-cleanliness, and purity.  EN DIN 1.2367 features high isotropy, reason for which transversal resilience is often three times higher when compared to conventional EN DIN 1.2367. Furthermore, the thermal fatigue resistance is also often much higher than that of conventional hot work tool steel EN DIN 1.2343, enabling longer die lifetime.

Steel Properties

- Small dimensional variation

- Impact resistance at high temperatures

- Good machinability

- Excellent high temperature strength and wear resistance.

- High hardenability and toughness.

- Tools can be water cooled.

Specifications

Chemical Composition

| Element | Percentage |
| --- | --- |
| C | 0.35-0.45 |
| Si | 0.20-0.50 |
| Mn | 0.20-0.40 |
| Cr | 4.80-5.50 |
| Mo | 2.80-3.50 |
| V | 0.50-0.80 |
| P | ≤0.030 |
| S | ≤0.030 |

Mechanical Properties:

| Property | Value |
| --- | --- |
| Hardness (HBW) | 229 max (Annealed) |
| Hardness After Quenching (hardenability) (HRC) | 50 min (Annealed) |
| Yield Strength | 1420 MPa |
| Elongation | ≥12% |
| Impact Toughness | ≥20 J |

Physical Properties

| Property | Value |
| --- | --- |
| Density (g/cm³) | 7.85 |

Modulus of Elasticity

| Temperature (°C) | GPa |
| --- | --- |
| 500 | 176 |
| 600 | 165 |

Thermal Properties

Thermal Expansion Coefficient

| Temperature (°C) | Thermal Expansion Coefficient (10^-6/°C) |
| --- | --- |
| 500 | 12.9 |
| 600 | 13 |

Thermal Conductivity

| Temperature (°C) | Thermal Conductivity (W/m·K) |
| --- | --- |
| 500 | 34.2 |
| 600 | 34.9 |

| Heat Treatment Process | Temperature (°C) | Duration | Cooling |
| --- | --- | --- | --- |
| Stress Relieving | 820 - 840 | 4-6 hrs | Furnace |
| Stress relief annealing | 600-650 | min 4 hrs | Furnace |
| Hardening | 1030 - 1060 | Group II | Oil, Air WB 500 - 550°C |
| Tempering | 500 - 700 See tempering curve | min 2 hrs Depending on cross section | Still air |

Applications

- Wear resisting tools

- forging dies,

- pressure die casting dies,

- pressing tools and extrusion dies for light and heavy metals, mandrels

- making inserts for light alloys die casting dies as well as for thermosets and thermoplastic injection moulding dies.

- closed dies, punches, stamps and jaws;

- hot rolling rolls, as well as hot cutting applications, such as circular cutting blades, straight cutting blades and angular cutting blades.

Quality Assurance

Our 1.2367 steel undergoes rigorous testing and quality control to meet international standards, ensuring consistent performance and reliability. Certificates and test reports are available upon request. Feel free to reach out to us for more information on our 1.2367 steel products or to discuss your specific requirements. We're dedicated to providing top-quality steel solutions that meet your needs and exceed your expectations.

MANUFACTURING RANGE

Products                             Diameter (mm)

Hot Rolled bar                       8 - 65

Forged and Turned bars        65.2 - 500

Forged Square Bars              50 - 500

FLATS

THICKNESS                     WIDTH

6.00 mm - 410.00 mm       20.00 mm  - 700.00 mm

Click here to contact our experienced sales team who will assist you with your 1.2367 tool steel enquiry.